Supporting Information

Synthesis of Perovskite-Type High-Entropy Oxides as Potential Candidates for Oxygen Evolution

Simon Schweidler1,*, Yushu Tang1, Ling Lin1, Guruprakash Karkera2, Alaa Alsawaf1, Lucile Bernadet3, Ben Breitung1, Horst Hahn1,4, Maximilian Fichtner1,2, Albert Tarancón3,5 and Miriam Botros1,*

1Institute of Nanotechnology, Karlsruhe Institute of Technology (KIT), Hermann-von-Helmholtz-Platz 1, 76344 Eggenstein Leopoldshafen, Germany

2Helmholtz Institute Ulm (HIU), for Electrochemical Energy Storage, Helmholtzstr. 11, 89081 Ulm, Germany

3Department of Advanced Materials for Energy, Catalonia Institute for Energy Research-IREC, C/Jardins de les Dones de Negre, 1, Planta 2 E-08930, Sant Adrià del Besòs, Barcelona, Spain

4KIT-TUD Joint Research Laboratory Nanomaterials Institute of Materials Science, Technische Universität Darmstadt (TUD), 64206 Darmstadt, Germany

5Catalan Institution for Research and Advanced Studies (ICREA), Passeig Lluís Companys 23, 08010 Barcelona, Spain

*corresponding authors:

simon.schweidler@kit.edu, miriam.botros@kit.edu

Table S1.Refined structural parameters a, b, c, V for HEO-La and HEO-Sr perovskite materials prepared by ball milling or Pechini method.

|  | HEO-La_BM | HEO-Sr_BM | HEO-La_PM; 900°C | HEO-Sr_PM; 900 °C | HEO-La_PM; 1200 °C | HEO-Sr_PM; 1200 °C |
| --- | --- | --- | --- | --- | --- | --- |
| Space group | Pbnm | Pbnm | Pbnm | Pbnm | Pbnm | Pbnm |
| a / Å | 5.3748(6) | 5.3554(4) | 5.3660(6) | 5.3211(7) | 5.3596(3) | 5.3310(9) |
| b / Å | 5.5534(7) | 5.5610(8) | 5.5057(5) | 5.4989(7) | 5.5007(3) | 5.4909(8) |
| c / Å | 7.6697(8) | 7.647(1) | 7.6382(7) | 7.584(1) | 7.6291(4) | 7.596(1) |
| V / Å3 | 228.93 (5) | 227.75(6) | 225.66(4) | 221.92(5) | 224.92(2) | 222.34(6) |

Figure S1. XRD patterns of HEO-La_BM and HEO-Sr_BM after calcination of the ball-milled synthesized materials at 1200 °C for 12 h.

Figure S2. Particle size distribution of HEO-La and HEO-Sr powders synthesized by ball milling and Pechini method.

Table S2. ICP-OES results for HEO-La synthesized using ball milling and Pechini method (SD = standard deviation).

| Element | Mass (Pechini) [wt.%] | n [mol] | SD [%] | Mass (BM) [wt.%] | n [mol] | SD [%] |
| --- | --- | --- | --- | --- | --- | --- |
| Gd | 14.01 | 0.21 | 0.09 | 13.43 | 0.21 | 0.15 |
| La | 11.90 | 0.21 | 0.02 | 11.36 | 0.19 | 0.06 |
| Nd | 12.16 | 0.20 | 0.07 | 10.08 | 0.17 | 0.11 |
| Sm | 14.92 | 0.24 | 0.09 | 14.17 | 0.23 | 0.15 |
| Co | 4.99 | 0.20 | 0.02 | 4.73 | 0.19 | 0.04 |
| Cr | 4.53 | 0.21 | 0.01 | 3.68 | 0.17 | 0.04 |
| Fe | 4.70 | 0.20 | 0.02 | 4.52 | 0.19 | 0.07 |
| Mn | 4.91 | 0.21 | 0.03 | 4.68 | 0.20 | 0.04 |
| Ni | 5.15 | 0.21 | 0.02 | 5.07 | 0.21 | 0.05 |
| Y | 7.96 | 0.22 | 0.02 | 7.53 | 0.20 | 0.06 |

Table S3. ICP-OES results for HEO-Sr synthesized using ball milling and Pechini method (SD = standard deviation).

| Element | Mass (Pechini) [wt.%] | n [mol] | SD [%] | Mass (BM) [wt.%] | n [mol] | SD [%] |
| --- | --- | --- | --- | --- | --- | --- |
| Gd | 14.84 | 0.22 | 0.10 | 14.26 | 0.20 | 0.28 |
| Sr | 7.74 | 0.20 | 0.10 | 7.41 | 0.19 | 0.25 |
| Nd | 12.91 | 0.21 | 0.12 | 10.90 | 0.17 | 0.34 |
| Sm | 15.83 | 0.24 | 0.14 | 15.02 | 0.23 | 0.42 |
| Co | 5.28 | 0.21 | 0.04 | 5.23 | 0.20 | 0.30 |
| Cr | 4.78 | 0.21 | 0.02 | 2.99 | 0.13 | 0.14 |
| Fe | 4.99 | 0.21 | 0.10 | 4.96 | 0.20 | 0.30 |
| Mn | 5.07 | 0.21 | 0.05 | 4.88 | 0.20 | 0.09 |
| Ni | 5.40 | 0.21 | 0.06 | 5.35 | 0.21 | 0.17 |
| Y | 7.91 | 0.20 | 0.06 | 7.44 | 0.19 | 0.20 |

Figure S3. HAADF images and EDX analysis HEO-La_BM.

Figure S4. HAADF images and EDX analysis HEO-La_PM. HEO-La_PM was calcined at 1200 °C for 12 h.

Figure S5. EDX spectra for a) HEO-La_BM, b) HEO-La_PM, c) HEO-Sr_BM and d) HEO-Sr_PM.

Figure S6. CV curves at different scan rates (5, 10, 20, 40, 60 mV s−1) of a) HEO-La_BM, b) HEO-La_PM, c) HEO-Sr_BM, and d) HEO-Sr_PM

Figure S7. LSV curves normalized to the ECSA.

Figure S8. LSV polarization plot toward the OER for different electrocatalysts in 1 M KOH at a scan rate of 5 mV s-1.