Supplementary Information

High-Throughput Synthesis of CeO2 Nanoparticles for Transparent Nanocomposites Repelling Pseudomonas aeruginosa Biofilms

Massih Sarif,1, † Olga Jegel,1, † Athanasios Gazanis,2 Jens Hartmann,1 Sergi Plana-Ruiz,1,3 Jan Hilgert,1 Hajo Frerichs,1 Melanie Viel,1 Martin Panthöfer,1 Ute Kolb,1,3 Muhammad Nawaz Tahir,4,5 Jörg Schemberg,6 Michael Kappl,7 Ralf Heermann2* and Wolfgang Tremel1*

1 Department Chemie, Johannes Gutenberg-Universität Mainz, Duesbergweg 10-14, D-55128 Mainz, Germany

2 Johannes-Gutenberg-Universität Mainz, Institut für Molekulare Physiologie, Mikrobiologie und Biotechnologie, Hanns-Dieter-Hüsch-Weg 17, D-55128 Mainz, Germany

3 Department of Materials and Geoscience, Technical University Darmstadt, Petersenstrasse 23, D-64287 Darmstadt, Germany

4 Chemistry Department, King Fahd University of Petroleum and Materials, Dhahran 31261, Kingdom of Saudi Arabia

5 Interdisciplinary Research Center for Hydrogen and Energy Storage (IRC-HES), King Fahd University of Petroleum and & Minerals, Dhahran 31261, Saudi Arabia

6 Institut für Bioprozess- und Analysenmesstechnik e.V., Rosenhof, D-37308 Heilbad Heiligenstadt, Germany

7 Max-Planck-Institute for Polymer Research, Ackermannweg 10, D-55128 Mainz, Germany

† these authors contributed equally to this work

Table S1. General information concerning the Rietveld refinement.

| General information | Description |
| --- | --- |
| Diffractometer Detector | Stoe Stadi P Dectris Mythen 1k |
| Wavelength (Å) | 0.7093 (MoKα1) |
| Temperature (K) Program | 298 TOPAS Academic 6.0 |
| Number of parameters Space group (cerianite) | 17 Fm-3m |
| Wyckoff positions | Ce: 4a, O: 9c |

Table S2. Information concerning the Rietveld refinement.

| Sample | Rwp | Cell parameter (Å) | Crystallite size (nm) |
| --- | --- | --- | --- |
| MF RT | 4.36 | 5.418(1) | 5.86(7) |
| MF 185 °C | 4.21 | 5.423(1) | 5.83(5) |
| MF 500 °C | 4.44 | 5.4141(2) | 16.2(1) |
| MF 800 °C | 8.70 | 5.41678(2) | 71.5(4) |
| Batch RT | 4.58 | 5.412(1) | 3.15(2) |
| Batch 185 °C | 4.28 | 5.417(2) | 3.78(3) |

Figure S1. (A) Setup for the segmented flow, (B) comparison of the reaction solution and the product. (C) CeO2 NPs after 83 minutes in the segmented flow and in the batch process.

Figure S2. HRTEM images of CeO2 NPs obtained under segmented flow conditions and annealed for 5 h at (A) 185 °C, (B) 500 °C and (C) 800 °C.

Figure S3. Michaelis-Menten kinetics for H2O2, with the corresponding Hill fit (red line) for the CeO2 NPs obtained from the segmented flow (A) annealed at 185 °C, (B) 500 °C and (C) 800 °C.

Figure S4. Contact angle measurements of polycarbonate with water (A) before and (B) after oxygen plasma treatment.

Figure S5. UV-VIS absorption spectra of polycarbonate before (black) and after coating (red) with CeO2 NPs.