# Supplementary material

Calculations:

The publications included in this review all provide their leaching efficiency. Thus, our definition of the corrected recovery efficiency for processes that include leaching is as follows:

| RRecovery,corrected=Rl· RRecovery100 |  | (4) |  |
| --- | --- | --- | --- |
| RRecovery,corrected | Corrected recovery efficiency |  | [%] |
| RL | Leaching efficiency |  | [kg] |

Table S. 1: Content of all reviews included in this review.

| Summary of content | Source |
| --- | --- |
| Recycling of LIBs and NiMH using minerals processing operations Description state of the art recycling technology (direct physical, pyro- and hydrometallurgical) Economics of battery recycling Proposed combined recycling process for a mixed feed of LIBs and NiMn Timeline of innovations of battery recycling processes | [16-18,121,222,235] [121,222][121,222][18 ,235][17,235][16] |
| Focuses on recycling of anode material and electrolyte Recycling capacity with recycling route Description state of the art recycling technology (direct physical, pyro- and hydrometallurgical) Regeneration of anode material and application of recovered anode material Processes for electrolyte extraction Industrial implementation LCA modeling approaches | [96,121] |
| Focuses on hydrometallurgical process Provides environmental and economical perspective Describes different commercial processes | [50,121] |
| Focuses on pyrometallurgical recycling of LIB, Ni-Cd and Ni-MH | [35,121] |
| Evaluation of sustainable benefits of LIB recycling Description state of the art recycling technology (direct physical, pyro- and hydrometallurgical) Battery marking for the identification of the cathode material by means of Battery identity global passport | [121,258] |
| Focuses on pyro- and hydrometallurgical processes Detailed battery composition Describes different commercial processes Discusses robustness and economics | [121,259] |
| Perspective on needs of finding solutions on the growing amount on end of life LIBs Market and global mining of resources Repurposing LIBs Description state of the art recycling technology (direct physical, pyro- and hydrometallurgical) | [97,121] |
| Description state of the art recycling technology (direct physical, pyro- and hydrometallurgical) Development of the LIB technology Hazards in LIB recycling processes such as thermal runaway Integrating pyro- and hydrometallurgical route in circular economy | [98,121] |
| Recycling processes for lead-acid, Ni-MH and LIB Description state of the art recycling technology (direct physical, pyrometallurgical) | [121,233] |
| Description state of the art recycling technology (direct physical, pyrometallurgical and hydrometallurgical) Energy consumption of recycling processes | [15,121] |
| Economic impact of LIB recycling Description state of the art recycling technology (direct physical, pyrometallurgical and hydrometallurgical) Emission reduction due to recycling Elemental composition Implementation of recycling Legal framework | [3,121] |
| Environmental and social impact of lithium ion batteries Disassembly of different EV LIBs Description state of the art recycling technology (direct physical, pyrometallurgical and hydrometallurgical) Comparison matrix of different process parameters and material recovery of the recycling routes | [17,121] |
| LIB composition LIB market Industrial implementation | [99,121] |
| LIB market development Industrial implementation Description state of the art recycling technology (direct physical, pyrometallurgical) | [18,121] |
| Focuses on hydro-metallurgical and direct physical recycling Review on Life Cycle Assessments Comparison matrix of different process parameters and material recovery of the recycling routes Evaluating process parameters Industrial implementation Process routes from different technical papers | [22,121] |
| Historical development of Lis Description state of the art recycling technology (direct physical, pyrometallurgical and hydrometallurgical) Presenting research of anode and electrolyte Industrial implementation | [121,229] |
| Focuses on the environmental impact of hydrometallurgical recycling with organic acids Life cycle assessment over the different life stages | [105,121] |
| Beside recycling discusses design and re-use Description state of the art recycling technology (direct physical, pyrometallurgical and hydrometallurgical) Industrial implementation | [121,260] |
| Development of LIB market Industrial implementation Description state of the art recycling technology (direct physical, pyrometallurgical and hydrometallurgical) With focus on hydro-metallurgical route | [74,121] |
| Focuses on the industrial implementation of hydrometallurgical process | [75,121] |
| Discusses resource scarcity Environmental hazards during landfilling Environmental impact during production Industrial implementation of recycling processes | [33,121] |
| Description state of the art recycling technology (direct physical, pyrometallurgical and hydrometallurgical) | [121,261] |
| Waste hierarchy Policy on different life stages Policy on different end of life scenarios | [104,121] |
| Lithium ion battery models in cars Fire hazards Description state of the art recycling technology (direct physical, pyrometallurgical and hydrometallurgical) Legal framework | [103,121] |
| Focusing on direct physical recycling | [102,121] |
| Industrial implementation of recycling processes Policy recommendation | [92,121] |
| Industrial implementation of recycling processes Energy recovery through discharging Hazards through battery recycling | [38,121] |
| Umicore Battery recycling EU Recycling Regulations on LIB Umicore recycling efficiency | [121,262] |
| Hazards through battery recycling Description state of the art recycling technology (direct physical, pyrometallurgical and hydrometallurgical) Patent publications on LIB development | [78,121] |
| LIB impact on society and economy Challenges in LIB recycling Industrial implementation of recycling processes | [26,121] |
| Description state of the art recycling technology (direct physical, pyrometallurgical and hydrometallurgical) LIB market and development EoL volume flow of LIBs Industrial implementation of recycling processes | [209] |
| LIB composition Hazards through battery recycling Waste management scenarios Environmental impacts of disposal Worldwide regulations on battery collection Description state of the art recycling technology (direct physical, pyrometallurgical and hydrometallurgical) LCA | [210] |
| LIB market development Description state of the art recycling technology (direct physical, pyrometallurgical and hydrometallurgical) LCA on different cell chemistry and recycling routes Waste management systems Chronological information on legal regulations | [263] |
| Description state of the art recycling technology (direct physical, pyrometallurgical and hydrometallurgical) | [44] |
| LIB composition LIB market development Research interest Description state of the art recycling technology (direct physical, pyrometallurgical and hydrometallurgical) Challenges in battery collection | [45] |
| Legal framework worldwide Description state of the art recycling technology (direct physical, pyrometallurgical and hydrometallurgical) | [86] |
| Development of the EV market Structure and composition of LIB, Pb-acid, Ni-MH, Ni-Cd Description state of the art recycling technology (direct physical, pyrometallurgical and hydrometallurgical) Focuses on hydrometallurgical Electrolyte recycling Industrial implementation LCA Chronological regulations | [28] |

Table S.  2: Number of publications found for each combination of subject (single processes, complete recycling process and investigated parameters) and methodology: technical paper (a), life cycle assessment (LCA) (b), reviews (c) and publications by recycler (d).

| Area/Criterion | Technical Paper a | Review c=a+b | LCA b | Company technical information |
| --- | --- | --- | --- | --- |
| Status of Development |  |  |  |  |
| Technical Readiness Level | 0 | 1 | 0 | 2 |
| Recycling Capacity | 1 | 10 | 0 | 6 |
| Research Interest | 149 | 0 | 0 | 0 |
| Process Performance |  |  |  |  |
| Process Steps | 60 | 17 | 0 | 3 |
| Recycling Efficiency | 34 | 2 | 0 | 1 |
| Process Energy | 35 | 7 | 0 | 2 |
| Environmental impact |  |  |  |  |
| CED | 0 | 17 | 17 | 0 |
| GWP | 0 | 23 | 22 | 0 |
| Pollution |  |  |  |  |
| Air Pollutants | 43 | 13 | 2 | 2 |
| Wastewater | 43 | 10 | 0 | 1 |
| Solid Waste Materials | 17 | 5 | 0 | 1 |

Table S.  3: Capacities, types of batteries that are recycled and recycling efficiency of commercially applied processes.

| Company | Capacity [t · a-1] | Types of recycled batteries | Recycling Efficiency | Founding | Other company purposes | Source |
| --- | --- | --- | --- | --- | --- | --- |
| Direct physical route |  |  |  |  |  |  |
| AkkuSer Oy | 4,000 | Portable spent batteries | 90 % | 2006 | no | [26,33,50,206,207] |
|  | <300 (LIB) |  |  |  |  | [208,209] |
| Retriev Technologies (formerly TOXCO) | 3,500 | NiCd, NiMH, LIB, Alkaline | - | “over 25 years” | no | [99,210, 264] |
|  | 4,500 |  |  |  |  | [33,50, 207,229, 265] |
|  | <300 (LIB) |  |  |  |  | [76,209] |
| SNAM | 350 | NiCd, NiMH, LIB | “up to 80 %” | 1941 | Energy group | [50,206, 264,266] |
|  | 300 |  |  |  |  | [50,207, 210,229, 265] |
| Pyro-metallurgical Route |  |  |  |  |  |  |
| Umicore | 7,000 (Belgium) 5,000 (China) | LIB, NiMH | 50 – 61 | 1989 | Mining, Recycling | [33,232, 259] |
|  | 7,000 |  |  |  |  | [50,96,97,207,210, 229] |
|  | >4,000 (LIB) |  |  |  |  | [267] |
| Accurec | 6,000 | NiCd, NiMH, LIB | - | 1995 | no | [207,229] |
|  | 5,000 (LIB) |  |  |  |  | [267] |
|  | 4,000 |  |  |  |  | [210] |
|  | 2,500 (LIB) |  |  |  |  | [264] |
|  | 1,000 |  |  |  |  | [99] |
| Glencore Plc. (formerly Xstrata) | 7,000 | LIB | - | 1974 | Mining and commodity trading | [207] |
|  | >4,000 (LIB) |  |  |  |  | [264] |
|  | 3,000 |  |  |  |  | [99] |
| Nickelhütte Aue | 3,000 | LIB, NiMH | - | 1635 | Mining and recycling | [208] |
| Sumitono-Sony | 120-150 | LIB, NiMH | - | 1919 | commodity trading | [50,207, 210,229, 265] |
| Eramet/Valdi | 20,000 | n. a. | - | 1880 | Mining | [207] |
| Brunp | 6,000 | NiMH, NiCd, LIB | - | - | Recycling | [208] |
| Dowa Eco-System | 1,000 | LIB | - | 1884 | Waste treatment | [207] |
| EcoBat (formerly G&P Batteries) | 145 | n. a. | - | - | Battery recycling | [207] |
| JX Nippon Mining and Metals | 5,000 | LIB | - - | 2010 | Mining | [207] |
|  | 5,500 | Ni-Cd; Ni-MH, LIB, industrial Alkaline Batteries |  |  |  | [268] |
|  | 5,000 |  |  |  |  | [50] |
| Batrec Veolia | 1,000 | NiMH, NiCd, LIB | - | 1992 | Battery recycling | [264] |
|  | 200 |  | - |  |  | [207] |
| Inmetco | 6,000 | Alkaline, NiCd, LIB | - | 1978 | Recycling | [229] |
| GEM High-Tech Co. (Eco-manufacture Hi-Tech Co.) | 100,000 | LIB and further battery types | - |  | Mining | [269] |
|  | 20,000-30,000 (LIB) |  |  | 2001 |  | [33,50, 207,208, 229] |
|  | 2,000-3,000 |  |  |  |  | [265] |
| Hyro-metallurgical route |  |  |  |  |  |  |
| Euro Dieuze/SARP | 200 | LIB | - | - | Chemical industry | [207] |
| Hunan BRUNP | 3,600-10,000 | LIB | - | - | Recycling | [207] |
| Recuply Valibat | 110 | LIB | - | 1993 | Recycling | [207] |
|  | <300 (LIB) |  |  |  |  | [267] |
| Bangpu Ni/Co High-Tech Co. | 3,600 | n/a | - | n/a | No | [229] |
| Duesenfeld GmbH | 1,500 | LIB | 91 | n/a | No | [211] |
| Green Eco-manufacture Hi-Tech Co | 20,000-30,000 | LIB | n/a | n/A | No | [230] |

Table S.  4: Cyclability experiments [23,25,93,180,192]

| Group | Cathode material | Cycles | Discharge rate | Initial charge capacity | Cathode cyclic capacity | Capacity change | Discharge capacity | Further information | Source |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Core refinement | LFP | 50 | 0.2 C |  |  |  | 120.03 mAh/9 |  | [192] |
| Core refinement | Mixed cathode materials | 200 | Up to 1 C |  |  | 4.5 % | 40.6 Ah | Pristine cell 42.5 Ah Coulombic efficiency 99.7% | [23] |
| Refinement | LCO | 16 | 0.5 C |  | 121.6 mAh/g | -0.54 %/Cycle | 142.4 mAh/g |  | [25] |
| Core refinement | NMC (unheated) | 80 |  |  |  |  | 147 mAh/g | „Excellent cycle life“ | [180] |
| Refinement | LFP |  | 0.5 C | 169.2 mAh/g |  |  | 164.5 mAh/g | „good cycling stability“ | [93] |

Table S.  5: Pollution to air, wastewater and solid waste materials of the different LIB recycling routes.

| Emission to air |  |  |
| --- | --- | --- |
| Pre-treatment |  |  |
| Quote | Remarks on Process | Source |
| „Pyrolysis products from the organics in electrode materials were taken out of the tube by nitrogen flow, and pyrolysis oils were then collected by condensation, while organic gas was collected and treated by a gas collector system. Deionized water and an NaOH solution were used to remove the acidic gas.” | Pyrolysis as pretreatment to recover anode and cathode material | [32] |
| “Due to the characteristics such as small particle size, simple chemical structure and low content, the outer solid organic compounds could be easily changed into gas with pyrolysis, and LiCoO6 and graphite without coating layer would be obtained.” | Pyrolysis as pretreatment to recover anode and cathode material | [191] |
| „The contemporary applied carbonates of the electrolyte (e.g. dimethyl carbonate and ethyl methyl carbonate) are flammable and contribute to the fire and explosion hazard. The highly flammable reaction products, like methane, ethane, and propene can cause fire and explosions. The chemical hazard could be induced by toxic gaseous reaction products like carbon monoxide (CO) and hydrogen fluoride (HF) resulting from the decomposition of the state of the art conducting salt lithium hexafluorophosphate (LiPF6) and the binder PVDF.“ | Pyrolysis as pretreatment to recover anode and cathode material | [51] |
| “During the oxygen free roasting between 873 K and 1273 K, the binder was evaporated and converted into gaseous products such as ethanol, ethyl, ethylene and benzene as shown in Figure 8(a). Besides, the gas production was quite low in this process. After the reaction, these gaseous products can be collected to use as clean energy to avoid disposal cost.[40, 46]” | Pyrolysis as pretreatment to recover anode and cathode material | [43] |
| “As in the LiCoO2 concentrate, only the organic outer layer could be burnt, the generated gas during roasting process was analysed by IR.” | Pyrolysis as pretreatment to recover anode and cathode material | [182] |
| “Gas pyrolysis products could be taken out of the tube by nitrogen flow, and then, macromolecular organics could be collected by condensation while small molecule organic gases were treated by a gas-treating system.” | Pyrolysis as pretreatment to recover anode and cathode material | [27] |
| “The pyrolytic gas was mainly composed of light alkenes, and the pyrolytic tar was mainly composed of aromatic long chain alkenes and light alcohols.” | Pyrolysis as pretreatment to recover anode and cathode material | [34] |
| „Although moderate roasting can remove organic compound layer on the particle surface to improve flotation effect, harmful ingredients would volatilize and produce irritating gases, such as HF, P2O5, and aldehydes under high temperature circumstance [19].“ | Pyrolysis as pretreatment to recover anode and cathode material | [85] |
| “operation, thermal treatment has also been widely used in WEEE treatment to burn PVDF binder and then separate Al/Cu foils and LiCoO2/graphite. At the same time, some harmful exhaust gases are produced from combustion of carbon and organic compounds in calcination processes, so that corresponding purification equipment should be adopted to prevent environmental pollution.” | Pyrolysis as pretreatment to recover anode and cathode material | [86] |
| “The pyrolysis products at a temperature of 500 °C, including the pyrolysis oils and gas, were mainly from the organic binders and electrolyte.” |  |  |
| “Non-condensable gases were extracted by vacuum pump and collected by the gas collector finally.” | Pyrolysis as pretreatment to recover anode and cathode material | [152] |
| “In this process, the binder is evaporated and decomposed into gaseous products which can be collected to avoid disposal cost.” | Oxygen free roasting | [43] |
| “The gaseous products such as ethanol, ethyl, ethylene, and benzene were collected and used as clean energy after pyrolysis in Figure 1b.” | Pyrolysis pre-treatment | [205] |
| “The off gases were purified in a system that consisted of a cooler, a condensation chamber, filters with activated carbon for heavy metals removal and bag filters.” | Pyrolysis as pretreatment | [64] |
| „The volatiles entered the condensers and were condensed, while the non-condensable gases were extracted by vacuum pump and collected by the gas collector finally.” | Pyrolysis as pretreatment | [77] |
| “CO2 gas is released during high temperature sintering, leading to the formation of porous products with rough surface morphology and clearly visible primary particles.” | Pyrolysis as pretreatment | [82] |
| “At the cell's negative terminal (cathode for aqueous solute electrochemical reactions), the vast majority of the solutes, particularly the Na+ and K+ ones, evolve hydrogen gas according to Eqs. (5) or (2) depending on the pH of the solution and the balancing equation at the other electrode.“ (NH4)2SO4 brine: “Since they are both competitive with each other, a mix of both gases may be expected to be produced, but both are significantly toxic, and often referred to as NOx. The two competing cathodic reduction reactions.” „Eq. (13), with the highest half-cell potential of +0.15 V, also produces a nitrogen oxide, N2O, otherwise known as nitrous oxide/laughing gas. N2O is far less toxic than NOx for the environment, less flammable, and less dangerous to human health.“ Chlorine anion brine: “For the halides, the competing reactions appear to be relatively competitive (Eq. (15)–(18)), although it would appear that chlorine oxidation to chlorine gas (Cl2 requires a larger potential than oxygen evolution in both acidic and basic solutions, but they are close enough in acidic solutions (only 0.13 V more positive) to mean that significant quantities of both can be generated.” Nitrite anion brine: “The final set of equations are related to ammoniumcation (NH4+) oxidation. Eq. (25) gives an example of direct oxidation to generate nitrogen gas at a slightly more negative potential than water oxidation (−0.77 V vs −0.40 V), which should occur only in basic solutions.” | Discharging in brine with different brines | [149] |
| “Brine discharge electrolyses the water, producing hydrogen and chlorine gasses, which are flammable and toxic respectively, although evolved chlorine will chlorinate the water it is in.” | Discharging in brine with different brines |  |
| “The off gases were purified in a system that consisted of a cooler, a condensation chamber, filters with activated carbon for heavy metals removal and bag filters.” | Pyrolysis of the binder | [62] |
| “The gaseous products during pyrolysis were analyzed by gas chromatography–mass spectroscopy [43]. The decomposition of polyvinyl alcohol (PVA, [C2H4O]n) binder at 600 °C, resulted in the main products of CO, CO2, C2H4, with small amounts of C2H5OH, CH3CHO, and C6H6.” | Pyrolysis of the binder | [43,261] |
| “Nevertheless, since it is not entirely possible to rule out the formation of chlorine gas from the NaCl solutions, a different approach is evaluated in the following Section to use sulfate salt solutions with the aim of eliminating the accumulation of precipitate on the electrode reactive sites.” | Discharging with salt solution | [174] |
| “Oxygen, hydrogen and other gases, such as chlorine (depending upon the salts in the brine), will form at the anode and cathode terminals, and can potentially be collected, though the dangers and difficulties associated with this should not be underestimated.” | Discharging with salt solution | [17] |
| “Advantageously, such an energy recovery process would not need to dispose of any gases evolved from the electrolysis of salt solutions, and would be able to discharge to a 0% state of charge, without overdischarging, dissolving the Cu current collector, and contaminating the waste streams.” | Discharging with energy recovery | [102] |
| “Compositions and amounts […] of the recovered electrolytes from commercial 18,650 cells after formation extracted with liquid CO2 and additional solvents for 30 min, with subsequent 20 min without additional solvent. Red, top: LiPF6; blue, below: ethylene carbonate (EC); yellow, middle: ethyl methyl carbonate (EMC); magenta, bottom: dimethyl carbonate (DMC).” | Electrolyte extraction with supercritical CO2 | [72] |
| “At the end of the extraction, the gas was separated from the solution, which was collected in a flask (Extracted sample, Fig. 1), while the gas passed through a washing step with sodium hydroxide solution” | Supercritical fluid extraction | [125] |
| Direct Physical |  |  |
| Quote | Remarks on Process | Source |
| “The volatized organic electrolyte was condensed by a condensation tube, and the tail gas was washed by NaOH solution at the end of the process.” | Crushing under nitrogen atmosphere | [34] |
| “To collect the gas released from dismantled LIB belts, a set of gas collecting system devices was designed independently. Two predominant organic vapour compounds were dimethyl carbonate (4.298 mg h_1) and tert-amylbenzene (0.749 mg h_1) from one dismantled battery cell.” “Gas containing VOCs of LIB went to the second sorbent sampling tube-14. The capacity emission container was 6.2 L, pneumatic pump capacity was 1 L min_1, the operating temperature of flat heater was set to 20 °C, the fan speed was set to 200 RPM.” | Pretreatment | [135] |
| “Disadvantages are on the one hand the energetic and chemical effort as well as the exhaust gas and chemical impact and on the other hand the fact that the wanted metals have to be extracted, whereby the metals become source materials at the end of the process.” | Electro hydraulic fragmentation | [168] |
| “The supercritical carbon dioxide extracts the electrolyte (ethyl methyl carbonate, diethyl carbonate, and LiPF6) from the cells, and is removed. The electrolyte separates from the gaseous CO2, and after further processing, can be recycled for use in batteries if it is determined to be economic.” | Review on recycling technologies | [233] |
| “Als Produkte entstehen so zunächst die leicht-flüchtigen Elektrolytbestandteile, welche einer Abgasreinigung zugeführt werden sowie eine FF1 < 1,0 mm.“ Translation: The first byproducts are the volatile electrolyte components, which are fed to a waste gas purification system, and an FF1 < 1.0 mm. | Exhaust gas cleaning after crushing | [14] |
| „Mechanical technology has the advantages of high efficiency and improved environmental properties (without generating wastewater and hazardous gas)” | General information | [164] |
| “Mechanical methods are simple and suitable processing but cause the release of toxic gases and lack of ability to separate all of the battery components.” | General Information | [50] |
| “After discharging, dismantling and an inert shredding process, the material is dried and the exhaust gases are cleaned using a combination of condensation and adsorption steps.” | Exhaust gas cleaning after crushing | [186] |
| „The grinding and drying stages are flushed with an inert drying gas producing an offgas loaded with different organic solvent components.” | Exhaust gas treatment of fixed-bed adsorber | [181] |
| „Das elektrolytbeladene Abgas soll mit Adsorption gereinigt werden und die Elektrolyte ggf. wiedergewonnen werden.“ | Exhaust gas treatment after crushing and drying | [21] |
| “The batteries are then shredded and immersed in water. Lithium ion/metal react with the water to produce lithium hydroxide and hydrogen gas, which is burned above the solution [8].” | Retrieve Process | [38] |
| “This wet crushing leads to decreased reactivity of the battery cells and avoids harmful emissions.” | On the retriev process | [51] |
| “Another key challenge to be addressed in scale-up is the emission of organic electrolyte. In this paper, it was evaporated under a fume hood, however, in an industrial shredding setting, it could produce hazardous air pollutants (HAPs) that need additional treatment. Many industrial shredding centers are beginning to make use of emission controls such as enhanced air handling and suction systems like cyclones, scrubbers and baghouse filters (McGlothlin, 2011; Al-Salem et al., 2009).” | General information | [184] |
| “This grinding flotation method is a promising separation method without any toxic emissions or introducing other impurities in industrial application.” | Flotation to separate anode and cathode material | [187] |
| “A sample (50 kg) of LIBs collected by S.E.V LTD. (Colico –LC Italy) was processed by an automated pre-treatment pilot plant equipped with gas treatment section (gas scrubber and carbon filters) and made up of a series of operations including crushing, sieving, magnetic separation, and eddy currents.” | Mechanical pre-treatment | [47] |
| “Batrec Industrie AG employs a hydrometallurgical process to recycle LIBs. The used batteries are sorted and crushed in a CO2 atmosphere, and the released lithium is then neutralized by moist air. Following crushing and neutralization, the protective CO2 gas is purified in a gas scrubber before being exhausted.” | Batrec Industrie AG | [97] |
| “Bartec [sic!] is one of the recycling processes developed to recycle mixed type of batteries. It includes crushing the spent batteries in CO2 gas atmosphere to liberate battery component and remove the volatile electrolyte as condensate (Georgi-Maschl era et al., 2012).” | BatRec | [36,222] |
| “Naturally occurring gases, H2 and O2, are extracted and filtered using a cyclonic system.” | Akkuser process | [26] |
| “In this process two crushing step at low and high speed rotary shredder was performed while the crushing system was inserted in a sealed medium filled with a mixture of Wie CO2 and argon. Crushing in inert gas expel oxygen and nitrogen and formed less reactive lithium carbonate.” | Recuply | [222] |
| “Meanwhile, the offgas from the crushing process is neutralized with water and soda.” | Recuply Process | [33] |
| Meanwhile, because of the violent friction and high-speed impact of crushing, this process can increase the temperature to as high as 300 °C. As a result, the electrolyte can easily decompose and volatilize to generate toxic gas, even HF if humidity is present. Diekmann et al. investigated the gas components released during crushing and showed that the electrolyte components, including solvents and salts, as well as the state of health (SOH) of spent LIBs greatly influenced the final released gas, as shown in Fig. 6a and b. Dimethyl carbonate (DMC), ethyl methyl carbonate (EMC), and CO2 were the main gas components released during crushing. | Exhaust gas during crushing | [28] |
| “recy- cling electrolyte materials and removal of these components will reduce the risk of fluoride gas emission in thermal pro- cessing.” | Electrolyte recovery | [33] |
| Pyro-metallurgical |  |  |
| Quote | Remarks on Process | Source |
| „Das Fluor aus dem Leitsalz LiPF6 stellt bei einer pyrometallurgischen Aufbereitung keine Probleme dar, da es als Calciumfluorid (CaF) bei einer Rauchgaswäsche abgetrennt werden kann.“ Translation: The fluorine from the LiPF6 conducting salt does not cause any problems in pyrometallurgical processing, since it can be separated as calcium fluoride (CaF) in a flue gas scrubber | General information | [14] |
| „Thermal treatment of charged LIBs requires an off-gas treatment system to avoid harmful emissions.“ | General information | [33] |
| „Wastewater, waste gas, and solid waste are generated during recycling processes. A strict three-waste monitoring and treatment system should be established to prevent secondary pollution and realize environmentally friendly recycling and utilization of spent LIBs. For the pyrometallurgical process, treatment of exhaust gases and solid waste must be considered. For high temperature processes, a well-designed furnace with an exhaust gas treatment device is essential to reduce risk. “ | General information | [197] |
| „The furnace requires offgas treatment to prevent toxic gas emissions (e.g., dioxins and furans).“ | General information | [33] |
| “Thermal treatment is simple operation and high throughput, but the energy consumption, gas emissions and investment emissions are very high in these methods.” | General information | [50] |
| “Hazardous emissions must be removed with flue cleaning systems to meet stringent environmental regulations.” | Gernal information | [74] |
| “The contemporary applied carbonates of the electrolyte (e.g. dimethyl carbonate and ethyl methyl carbonate) are flammable and contribute to the fire and explosion hazard. The highly flammable reaction products, like methane, ethane, and propene can cause fire and explosions. The chemical hazard could be induced by toxic gaseous reaction products like carbon monoxide (CO) and hydrogen fluoride (HF) resulting from the decomposition of the state of the art conducting salt lithium hexafluorophosphate (LiPF6) and the binder PVDF.” | General information on thermal runaway | [51] |
| “Hazardous emissions must be removed with flue cleaning systems to meet stringent environmental regulations.” | General information | [33] |
| „The organics, lithium, and fluoride in the batteries are lost as fly ash and are removed from the flue by a scrubbing system.“ | On the Sony-Sumitomo process | [38] |
| “The offgas from the rotary hearth furnace is scrubbed, and the scrub solution is sent to a wastewater treatment facility to recovery cadmium, zinc, and lead.” | Inmetco gas treatment | [33] |
| “In the plastic pyrolyzing zone, plastics in the battery packs melt, oxidize, and provide energy to the offgas. […] The offgas from the furnace is heated by a plasma torch to above 1150 °C and sent to a post-combustion chamber, where halogens are captured by injection of calcium or sodium-based products or zinc oxide. Then the offgas is quickly cooled down by water vapor to avoid recombination of organic compounds with halogen or formation of dioxins and furans [52].” | Umicore gas treatment | [33] |
| “The Umicore process pays special attention to the exhaust gases. For example, the mid-section exhaust is recirculated into the low-temperature section, aiding with the electrolyte evaporation and reducing energy consumption. Additionally, the exhaust gases of the high temperature section are cooled down to avoid the formation of dioxins and furans, and are finally filtered [40,77].” | Umicore gas treatment | [26] |
| “However, a series of chemical reactions of hydrolysis, oxidation and decomposition, produces a negative carbon dust, alkali and heavy metal ions, may cause heavy metal pollution and dust pollution, when the electrode materials [sic!] of spent LIBs go into the environment [8–10]” | Flue dust pollution during LIB recycling | [37] |
| “The exhaust gases from incineration were washed in a gas scrubber filled with a potassium hydroxide solution.” | Exhaust gas cleaning after calcination | [166] |
| The vaporized solvents can be recovered by condensation or combusted via a thermal post-combustion process which regains the thermal energy. Additionally, the conducting salt LiPF6 is decomposed while generating HF as a gaseous product. HF leads to the necessity of a gas scrubber application. | Post combustion process of electrolyte | [51] |
| Although a large number of toxic gases will be generated at 800 °C, the secondary combustion and rapid cooling system of exhaust gas, which has been widely used for industrial waste incineration, can effectively remove the influence of toxic gases [19, 20] | Gas treatment | [42] |
| “At 800 °C, Li escaped from the sample in form of gas and cobalt oxide was completely reduced to the metallic cobalt.” | Binder decomposition | [201] |
| “The waste gas can be removed in a system, which consists of a cooler, a condensation chamber, and a limestone filter.33” | Molten salt process | [197] |
| “The off-gas is exhausted with a maximum flow rate of 5000 m3 h−1 and cleaned in a subsequent impact separator and an electrostatic precipitator.” | Review on the recycling routes | [36] |
| “Thus, Co and Li2CO3 can be the main solid products of the carbothermic reduction. LiCoO2 can react with C and CO and form Co, Li2CO3, and gases (CO and CO2), through the following reactions:” |  | [200] |
| “In the meantime, about 3.54% of weight loss was observed that is caused by gas emission originated from the decomposition of poly(vinylidene difluoride) (PVDF) binder and oxidization of the carbon content.” | Binder decomposition | [41] |
| „Verantwortlich sind die Emissionen säurebildender Abgase.“ Translation: The emissions of acid-forming exhaust gases are responsible. | LCA of EcoBatRec | [120] |
| “The offgas from the rotary hearth furnace is scrubbed, and the scrub solution is sent to a wastewater treatment facility to recovery cadmium, zinc, and lead.” | Inmetco | [33] |
| „A lithium enrichment can only be achieved in the flue dust and the slag has to be crushed and milled before leaching.“ Composition of flue dust | Lithium recovery from flue dust | [36] |
| Hydro-metallurgical |  |  |
| Quote | Remarks on Process | Source |
| “The Recupyl Valibat process conducts the recycling process under low temperature, making it easy to dispose of flue gas and H2.” | Recuply process | # [229] |
| “Notably, strong acid leachants release toxic gases like Cl2, SO3 and NOx and the waste acid solution is harmful to the environment. […]The three organic acids were selected because of their characteristics including easy natural degradation and the absence of toxic gases in the reaction process, and because of previous reports of other metal leaching processes.” | Organic acid leaching | [65] |
| “Inorganic acid leaching often results in secondary pollution with toxic gas, so increased attention has been given to environmental-friendly organic acid leaching, as shown in Table 1.” “The pretreatment process was conducted under sealed conditions to prevent electrolyte decomposition and alkaline gases from leaking into the environment.” | General information and pretreatment | [136] |
| „However, toxic gases like Cl2, SO3, and NOx are released in the process of extracting metal ions with inorganic acids, posing a serious threat to the environment.“ | General information and inorganic acid leaching | [197] |
| „The work aims at revealing issues, such as gas evolution during LIBs leaching, which may affect the feasibility of future LIBs treatment processes.“ “Through calculation with HSC Chemistry 9.4.1 (Outotec), we can show that reduction of chloride ions and release of chlorine gas is thermodynamically a viable reaction: 2LiCoO2s+8HClaq=2 LiCl aq+2CoCl2aq+Cl2g+ H2O(aq)” „Chlorine gas is a toxic molecule, which can be treated via adsorption and electrolysis (Jüttner et al., 2000). It is also industrially possible to reuse chlorine gas directly in hydrometallurgical processes (Anderson, 2014).“ | Leaching with HCl | [147] |
| “The liquid output materials are solutions of sodium hypochlorite and sodium chloride. Sodium hypochlorite was obtained by scrubbing free chlorine gas in sodium hydroxide solution which was released during manganese precipitation and it can be recycled in the process.” | Leaching with hydrochloric acid with gas clean up | [124] |
| „It is important to highlight that the industrial use of sulphurbased [sic!] compounds, such as the reducer used in this paper, is always subject to potential emissions of sulphurous gases. However, such compounds are widely used in several industries, including in hydrometallurgy. Therefore, special cares regarding gas emissions and their treatment are necessary, mainly at an industrial scale.“ “A gas treatment that could be adopted in the process proposed is the scrubbing in alkaline solutions, for example.” | Leaching with sodium metabisulphite | [79] |
| „The first one is the negative environmental effect caused by poisonous gases of Cl2 generated during leaching reactions, which should be seriously taken into consideration during leaching processes.” “Meanwhile, an increasing attention has been transferred to the application of different organic acids during the leaching processes due to the serious secondary pollution caused by strong mineral acids, such as poisonous gases, excessive waste acid and other unreacted solid wastes, which a further invest will be required for the alleviation and elimination of the potentially hazardous materials.” “One point in this case is the easy oxidation property of ascorbic acid in air atmosphere, in which itmay [sic!] react with oxygen in the air to degenerative acid and directly affect its leaching ability. Therefore, extra protection of inert gases may be required during the leaching processes, which may increase the cost during leaching.” “However, extra inert gases should be employed for the prevention of oxidation process when transition metals (Ni, Co and Mn) are exposed to the atmosphere for the transition metals can be easily oxidized into their high valences with their exposure to oxidant, such as O2 in the air.” | General information Inert atmosphere during leaching with ascorbic acid or during precipitation | [48] |
| “In terms of environmental point of view, the effluents generated are the gaseous, liquid and solid. The gaseous effluent of the process is nothing but oxygen leading to healthy environment to work.” | Electrochemical recovery | [148] |
| “In the process without cathode resynthesis, the acid used in the leaching process has acidification potential, especially the gases generated by inorganic acids. In this work, LiNi1/3Co1/3Mn1/3O2 was resynthesized to reduce the raw materials consumption, and the leachate are transformed into “gel” without producing effluent, acid or harmful gases, which has less impact on our environment.” | Gel formation | [242] |
| “Although HCl has a better leaching rate, it results in serious environmental problems and requires special equipment for treating chlorine (Cl2) gas, which will contribute to the recycling cost.” | Leaching with HCl | [161] |
| “Besides, almost no effluent, waste residues or exhaust gases will be produced during the closed-loop recycling process, indicating a “near-zero” pollutant emission process with remarkable environmental benefit.” | Closed loop process | [127] |
| “Compared with pyrometallurgy, hydrometallurgical processes produce lower amounts of waste gases and solid waste; however, wastewater generated by these processes requires consideration. Regulations should be formulated for wastewater recycling, such as purification of high concentrations of ions by reverse osmosis to achieve zero wastewater emissions. ” | General information | [94] |
| “Sodium hypochlorite was obtained by scrubbing free chlorine gas in sodium hydroxide solution which was released during manganese precipitation and it can be recycled in the process.” | Exhaust gas treatment | [124] |
| “In future developments, organic acids may be interesting as an environmentally friendly lixiviant that reduces the need for wastewater and gas treatment systems.” | General Inforamtion | [74] |
| Wastewater |  |  |
| Pre-treatment |  |  |
| “Deionized water and an NaOH solution were used to remove the acidic gas.” | Wastewater from pyrolysis | [32] |
| Composition of the brine | Discharging in brine | [135] |
| Direct Physical |  |  |
| “Physical separation processes (Al-Thyabat et al., 2013; He et al., 2017; Kim et al., 2004) require the minimal addition of chemical agents and generate relatively small amounts of waste water or gas.” | General Remark | [34] |
| “Although those processes can separate the active materials, most of them are expensive and have troubles in the disposal of waste water.” | Flotation | [192] |
| “In addition, how to reuse the waste water generated during flotation process to avoid secondary pollution is also an important research issue in the further.” | flotation | [167] |
| “Related to the relative high amount of process medium of 27 l per batch it was more suitable to use the sedimentation process with decanting the water.” | EHF process | [168] |
| “Furthermore, some wastewater was produced.” | Eddy current separation | [164] |
| “Furthermore, some wastewater was produced.” | Wet crushing | [190] |
| Pyro-metallurgy |  |  |
| Wastewater occurs during water leaching to recover manganese and lithium | Water leaching | [203] |
| Wastewater occurs during water leaching to recover manganese and lithium | Water leaching | [43] |
| Wastewater occurs during water leaching to recover manganese and lithium | Water leaching | [42] |
| Wastewater occurs during water leaching to recover manganese and lithium | Water leaching | [201] |
| Wastewater occurs during water leaching to recover manganese and lithium | Water leaching | [205] |
| “After calcination for 20 min, the roasted powders were washed by water (solid−liquid ratio: 100 g/L), and the wash liquid was retained for further processing.” | Water leaching | [197] |
| “Lithium extraction efficiency reached an optimal value which using a mass ratio of water/calcines of 30:1.” | Water leaching | [195] |
| “Calcines were cooled to room temperature. Subsequently, the above samples were ground for 20 min and leached with water at 30–90 °C for 20–120 min using water/calcine mass ratios of 10 : 1 to 50 : 1.” | Water leaching | [199] |
| Wastewater occurs during water leaching to recover manganese and lithium | Water leaching | [41] |
| “The leaching efficiency of primary valuable metals by carbonated water leaching (flow rate of CO2. 20 mL/min, liquid-solid ratio. 10:1, leaching time. 2 h, ambient temperature).” | Carbonated water leaching | [57] |
| “The offgas from the rotary hearth furnace is scrubbed, and the scrub solution is sent to a wastewater treatment facility to recovery cadmium, zinc, and lead.” | Wastewater from scrubbing | [33] |
| Hydro-metallurgy |  |  |
|  | Acidic wastewater | [77] [88] [79] |
| “In the process without cathode resynthesis, the acid used in the leaching process has acidification potential, especially the gases generated by inorganic acids. In this work, LiNi1/3Co1/3Mn1/3O2 was resynthesized to reduce the raw materials consumption, and the leachate are transformed into “gel” without producing effluent, acid or harmful gases, which has less impact on our environment.” | Gel formation | [242] |
| Several inorganic acids, such as HCl,17−19 HNO3,20−22 and H2SO4,23−27 have been used to leach metals from the cathodic materials of spent LIBs; however, these leachants release toxic gases during the process, thereby causing significant secondary pollution.28 |  | [56] [161] [91] |
| “On the other hand, inorganic acids may be corrosive and release toxic/harmful gases (eg, Cl2, NOx, SOx), and require additional wastewater processing costs (eg, neutralization and large volumes of water) to avoid secondary pollution.116” | Generel information | [74] |
| “Strong acids such as hydrochloric acids and nitric acid produce harmful fumes and gases such as Cl2, SO3 and NOx and, their waste solutions can penetrate to the soil and ground waters and cause damage to local people, biodiversity, and ecosystems (Li et al., 2013).” | Organic acid leaching | [130] |
| “The dissolution of metals also rose with the increase in the liquid/solid ratio (L/S), however, extractions above 85% can be reached at L/S as lower as 4.5 L/kg, which is favourable for further purification and recovery operations.” “It is important to highlight that the use of small amounts of acid, preferably near to the stoichiometric value, is desirable not only from the economic point of view of the consumption of reagents but also in order to simplify the treatment of final solutions and waste water.” | s/l ration with sodium metabisulphite | [79] |
| “Hydrometallurgy is a well-established process for the separation and recovery of metal ions, with such benefits as the complete recovery of metals with high purity, low energy requirements (Huang et al., 2009), the minimization of wastewater and no air emissions (Pietrelli et al., 2005).” “After filtration and washing with water for three times and then a black residue and a pink solution were obtained. Upon cathode leaching, the following operational variable were take into account to determine the optimum conditions: concentration of DL-malic acid (0.5–3.0 M), the amount of H2O2 (0–2.5 vol.%), solid/liquid ratio (33–17 g L_1), temperature (20 –100 _C) and reaction time (10–50 min).” | Leaching after pyrolysis | [242] |
| Wastewater composition is given | Electrochemical removal of lithium Wastewater composition | [132] |
| Wastewater composition is given | Lithium recovery from wastewater after RO treatment | [154] |
| Wastewater composition is given “On the other hand, in the case of oxalate recovery, metal- bearing solutions (Table 3, post CoC 2 O 4 solution) need further pro- cessing or wastewater treatment for oxalate removal.” | Oxalate leaching and Co, Ni and Li recovery | [47] |
| “In the ascorbic acid leaching, the following operational variable were investigated: temperature (30-90 °C), duration (5-50 min), concentration of ascorbic acid (0.3-1.5 mol/L), and solid/liquid (S/L) ratio (15-50 g/L).” | Ascorbic acid leaching | [137] |
|  | Recycling of wastewater | [89] |
| “Firstly, the existing hydrometallurgical processes may produce wastewater containing fluorine and pollute the environment due to the incomplete recycling of the organic binder and electrolyte (usually LiPF6, of high cost), and it is also difficult and expensive to treat the wastewater [4].” “2MH2SO4, 5 vol.%H2O2, leaching time of 60min, leaching temperature of 80 ◦C and solid/liquid ratio of 50 g/L. Without any fluoride removal treatments like addition of soluble calcium, the concentration of fluoride in the wastewater is measured below 3mg/L, which meets the Chinese regulatory let out concentrations in the “Generalized Sewage let out Criterion” (GB8979-96).” | Fluorine in wastewater | [152] |
| “From an environmental and health viewpoint, hydrometallurgical treatment is the favored technology for recycling of the metals from LIBs compared with pyrometallurgical and biometallurgical processes, because it offers such advantages as low energy consumption, no air emissions, complete recovery of valuable components with high purity, and the minimization of wastewater.” | General information | [67] |
| “However, these inorganic acid solutions produce leachates of low pH, posing a threat to the environment and making them unfavourable for subsequent waste water treatment (Yao et al., 2015).” “However, wastewater emission and complicated purification process make them uneconomic for the recycling process.” | General information | [158] |
| “Theoretically, waste water contained only Na3PO4 may be produced during the whole leaching and metal recovery process and Ca(OH)2 may be used for the removal of PO4 3_ and the regeneration of NaOH (2Na3PO4(a) + 3Ca(OH)2(a) -= 6NaOH(a) + Ca3(PO4)2 (s)).” | Wastewater composition | [101] |
| Table 3 Water 265-675 t/a | Wastewater consumption | [16] |
| “(1) a need for sorting, which requires increased storage space and adds to process cost and complexity; (2) the challenge of separating some elements (Co, Ni, Mn, Fe, Cu, and Al) in the solution, due to their similar properties, which can lead to higher costs; and (3) the expense of waste water treatment and associated costs.” “Secondary waste treatment: The waste in the hydrometallurgical process is water and chemicals fromthe leaching step, co-precipitation, and washing, which increase recycling costs. Further research on purifying the wastewater, reusing the water, or reducing the amount of water in the process is needed to reduce or eliminate waste water and associated costs.” | General information | [97] |
| “However, such advantages may be argued depending on flowsheet complexity, reagent schemes, effluent toxicity, and water consumption.” | General information | [22] |
| “More than 99% of Li is leached without the addition of acid and alkali under the optimal conditions of 1.05 times the stoichiometric amount of persulfate, under remarkably mild conditions (25°C, 20 min stirring a 300 g/L suspension of powdered cathode plates) with nearly no wastewater and solid waste generation.” | Lithium leaching | [75] |
| “Third, the wastewater containing strong acid from the leaching process must be treated before emission to avoid the secondary pollution. From the above, a further disposal of the hazardous gases, acidic leachates and acid wastewater is required and additional expenditure will be produced by using inorganic acids as leaching reagents.” | General information | [234] |
| “However, conventional inorganic acids produce leachates of low pH and inevitably introduce some secondary pollutants such as emission of Cl2, SO3, and NOx, posing a threat to the environment and making them unfavorable for subsequent waste water treatment.” “Since organic acid leaching liquors from spent LIBs contain valuable metals, complex purification process for separating metals from the solution is costly, and causes a significant concern of extra waste water emission.” | General information | [86] |
| Waste |  |  |
| Pre-treatment |  |  |
| “The pyrolytic gas was mainly composed of light alkenes, and the pyrolytic tar was mainly composed of aromatic long chain alkenes and light alcohols.” Provides composition “The images of spent the disposal devices of pyrolytic gas and tar are shown in Fig. 9, which shows that the steel strip furnace can deal with spent LIBs and make the separation of current collectors and active materials extremely easy.”LIBs pyrolysis in steel strip furnace, the pyrolysis residues, and | Pyrolysis as pretreatment to recover anode and cathode material | [34] |
| Direct physical |  |  |
| “First, disposable toxic 51 waste will be reduced to a minimal necessary amount.” | Reduction of waste | [134] |
| “The present recycling process is eco-friendly and highly efficient and produces little waste.” | General information | [13] |
| „The dissepiment can be directly recovered or disposed of by a downstream company.“ | Separators | [13] |
| “After the grinding step, the material was sieved in order to separate the powder fraction from the other materials. This step provided 330.7 g of powder (LiCoO2 and graphite) and 380.1 g of the other materials (external casing, Al, Cu, polymers and adhered waste powder).” | Spout bed procewss | [11] |
| Pyro-metallurgy |  |  |
| “There is still a lack of information on the generation of secondary waste during the thermal treatment, characterization of the waste and environmental risk assessment of the gas and oil products remaining after the incineration and pyrolysis. Despite the utilization of pyrolysis/incineration in the industrial LiBs recycling, conditions used are mostly applied as an estimation of the need to reach some processe efficiency, without the consideration of energy demand optimization or the adverse effects of the selected treatment on the material recycling efficiency and waste generation.” | Gerneral infromation | [200] |
| “At the end 34.51% of residues and losses are generated which, amongst others, include CO respectively CO2, slagged battery components and diffuse emissions like losses during charging or spillings during tapping of the electric arc furnace.” | Losses during pyrometallurgical process | [36] |
| “Also, this process does not recover other valuable metals such as lithium. Recovery of metals from the slag is energy intensive and not economical, and thus the slag is generally disposed or sold as construction material.” | Slag | [33] |
| “Lithium is lost in the fly ash and is not recovered.” | Dust | [210] |
| “In order simplify the research, a simulated slag is adopted in line with our previous work [33] with the following conditions: silica of 20–60 wt%, calcium oxide of 20–35 wt%, aluminium oxide of 10–30 wt% and lithium oxide of 0.5–15 wt% [39,40].” | Slag composition | [195] |
| Table 1 | Slag composition | [196] |
| Table 3 | Slag composition | [42] |
| Table 4 | Slag composition | [36] |
| Hydro-metallurgy |  |  |
| “Large volume of waste acid/alkali, heavy metal ions and negative carbon dust would be produced and may cause serious secondary pollution.” | General Information | [43] |
| “Waste products. The only waste product generated during the leaching step is water, eqn (2)–(5). When the metal hydroxides are precipitated sodium sulphate is generated according to eqn (9) and (10).” | No waste produced | [161] |
| Table 3 “solid waste and sludge disposal 40-120 t/a” | When processing 100-250 t/y process powder | [16] |
| “To increase the leaching efficiency, reductive leaching was carried out with H2O2 as the reducing agent. After leaching, the leaching solution and insoluble residue were separated by filtration.” | Residue on filter | [152] |
| “The insoluble residue was separated from the leachate by filtration.” Composition of the residue | Residue on filter | [156] |
| “After leaching, the insoluble residues and leachate were separated via filtering. The leachate was withdrawn to determine the concentrations of Mn, Li, Co, and Ni, and these data were used to calculate the leaching efficiencies.” | Filter residue | [56] |
| “Further, the leach residue was found to be graphite, which was confirmed by X-ray diffraction analysis.” | Filter residue | [124] |
| “After leaching, the resulting solution and insoluble residue were separated by filtration and washed with distilled water, yielding a pink filtrate and a black residue.” | Filter residue | [137] |
| “Fig. 5 demonstrates that the main phase of the leached cathode residue is graphite.” | Filter residue | [58] |
| “Residue (C-powder)” Fig. 2 | Filter residue | [89] |
| “The dissolution efficiency was optimized via removing insoluble impurities (e.g. residual graphite) and tuning the liquid–solid concentration acid ratio, reaction time, and temperature.” | filter residue | [90] |

Table S.  6: Process steps of the different LIB recycling routes with starting and ending point.

| No. of process steps | Starting point | Intermediate processes | Ending point | Remark |  | Source |
| --- | --- | --- | --- | --- | --- | --- |
| Direct physical |  |  |  |  |  |  |
| 6 | LIB | hammer mill 1st size separation 1st elutriation 2nd elutriation 3rd elutriation 2nd size separation | Powder (LCO + graphite) |  |  | [11] |
| 4 | Spent LFP batteries | discharging dismantling core crushing | Crushed products |  |  | [12] |
| 5 | Spent LFP batteries | perforation discharge disassembly thermal treatment inner core broken sieving | Carbon and lithium iron phosphate |  |  | [13] |
| 4 | Battery for recycle | shred screen physical processes relithiation | Cathode product | Comparing flow chart |  | [15] |
| 7 | LIB traction battery | disassembly discharging 1st shredding 1st classification Eddy current sorting 2nd shredding 2nd classification | Fine fraction (< 0.5 mm) | exhaust gas treatment electrolyte recovery |  | [14] |
| 6 | LIB | 2 rotors crushing sieving 1mm hammer crushing sieving 1 mm thermal treatment eddy current separator | Nonferrous metals, ferrous metals and non-metals | Mass balance |  | [16] |
| 3 | Batteries | high-airflow comminution 2nd comminution magnetic separation | Foils, anode and cathode | Comparing flow chart |  | [17] |
| 5 | Batteries | water spray or immersion comminution size separation dry thermal processing size separation froth flotation | cathode | Battery manufacturing included |  | [17] |
| 6 | Spent batteries | discharging disassembly extraction (electrolyte) size reduction physical separation relithiation | LiMn2O4 | Recovery of electrolyte Off gas cleaning |  | [18-20] [18] [19] [20] |
| 14 | Spent LFP batteries | discharging dismantling soaking in dilute NaOH solution mechanical separation smashing stirring in dilute NaOH solution washing centrifuging drying ball-milling sieving ball-milling sieving heat-treating | Repaired cathode powders | electrolyte recovery |  | [18] |
| 13 | Battery systems | system discharging disassembly cell discharge module discharging 1st shredding drying magnet separation 2nd shredding cyclone zig zag sifter fine dedusting sieving extraction with H2O | Wet active material |  |  | [21] |
| 9 | LFP pouch cells | discharge dismantling alkaline wash separation crushing alkaline wash milling sieving thermal treatment at 650 °C | Refreshed LFP |  |  | [22] |
| 6 | Spent NMC battery | discharge to 0.2 V manual opening alkaline wash at pH 10 pressure lithiation at 300 psi rinsing and drying at 120 °C thermal treatment at 900 °C | Refreshed NMC |  |  | [22] |
| 5 | Spent LFP battery | discharge to 0.5 V dismantling grinding relithiation for 20 h drying and grinding | LFP |  |  | [22] |
| 6 | LCO | dismantling discharge 1st separation step 2nd separation step Electrochemical resynthesis at 40 – 100 °C | LCO |  |  | [22] |
| 6 | Used single EV pouch cell | cell discharge disassembly rinsing with de-ionized water liberation sieving froth flotation | Cathode active materials |  |  | [23] |
| 4 | LIBs | hammer mill drying (80 °C/24 h) size separation electrostatic separation | Mixture (Metals + Polymers) |  |  | [24] |
| 6 | Batteries | extract shred sift/float heat 1 (hydrothermal) froth heat 2 (sinter) | Healed cathode |  |  | [25] |
| 5 | Spent LIB | hammer mill shaking table 105 µm screen thermal treatment 500 °C froth flotation | LiMeO |  |  | [26] |
| 5 | Spent LIB | disassembly liberation sieving froth flotation purification | New Li-ion battery | Battery manufacturing included |  | [29] |
| 5 | Spent LIBs | classification manual/auto dismantle crushing screening/sieving separation | n. a. | Overview flow chart |  | [28] |
| 6 | Spent LIBs | discharging manual dismantle separation mechanical separation PVDF elimination Al foil dissolution | n. a. |  |  | [28] |
| 8 | Spent LIBs | discharging shearing crushing impact crushing dry sieving grinding dry sieving surface modification flotation | LCO |  |  | [30] |
| 8 | Spent LIBs | discharging process mechanical shredding pneumatic separation magnetic/eddy current separation pyrolysis mechanical crushing sieving flotation | Cathode material | Organics recycling |  | [31] |
| 5 | Spent LIB | sorting by type disassembling autothermal pyrolysis multi-step mechanical processes vacuum evaporation or selective entraining gas evaporation of Li | Li, metal oxide | electrolyte condensation |  | [33] |
| 6 | Spent LIBs | Discharging Shredding Electrolyte extraction Electrode/metal separation Cathode and anode separation Cathode regeneration | Regenerated cathode material | Electrolyte recovery |  | [163] |
| 3 | Electrode | Detaching current collector Removing PVDF binder Separating active material and conductive additive | Active materials |  |  | [93] |
| 7 | Spent LFP | discharge crushing low temperature volatilization pyrolysis with nitrogen crushing screening flotation | LFP, concentration | Electrolyte recovery |  | [34] |
| 3 | Spent LIB | High airflow comminution Second comminution Magnetic separation | Black mass | Akkuser TRL ≥ 8 |  | [92] |
| 5 | Spent LIB | Wet comminution Density separation Mixing Filtration Drying | Black mass | Retrieve TRL ≥ 8 |  | [92] |
| Pyro-metallurgical route |  |  |  |  |  |  |
| 3 | LIBs | mechanical pre-treatment heat treatment at 150 - 500 °C heat treatment at 1,400 – 1,700 °C | Co-alloy, CoO, Co3O4, Li2O, Li2CO3, slag residue | Comparison of LIB, NiCd and NiMH | [35] |  |
| 3 | Battery for recycle | pyro-metallurgy leach solvent extraction | Dissolved salts | Overview flowchart | [15] |  |
| 6 | LIB scrap | pre-treatment vacuum-thermal treatment mechanical processing agglomeration pyro-metallurgical processing hydro-metallurgical processing | Co-based alloy, Li carbonate | Electrolyte recovery | [36] [18] |  |
| 2 | Batteries | pyro-metallurgy hydro-metallurgical extraction | n. a. | Overview flowchart | [17] |  |
| 8 | 18650 and laptop batteries | discharging scraping screening oxygen-free roasting wet magnetic separation magnetic force solution evaporation deposition | Co, Li2CO3, C |  | [37] |  |
| 7 | Spent batteries | sorting plastic removal calcination distillation shredding rotary-hearth furnace electric arc furnace | Slag, Fe/Ni alloy | Off-gas cleaning | [33] |  |
| 8 | Spent LIB | shredder hammer mill 707 µm screen mixing tank filter press evaporator mixing tank filter press | Li2O3 |  | [26] |  |
| 3 | Spent LIB | shaft furnace 300 – 1,450 °C leaching leaching | CoCl2 |  | [26] |  |
| 11 | Spent LIB | sorting dismantling vacuum thermal treatment milling grinding separation agglomeration process reducing meltdown leaching precipitation filtration | Li2CO3, Ni(OH)2 |  | [26] |  |
| 6 | Spent LiCoO2 cathode | crushing reductive roasting leaching of Li and Al leaching of Co purification evaporation & crystallization | CoSO4 |  | [40] |  |
| 4 | LiCoO2 | catalytic carbothermic reduction water leaching filtration washing | CoO & graphite |  | [41] |  |
| 6 | Spent LIBs | discharging dismantling drying roasting water leaching filtering | Co3O4 & Lithium ion solution |  | [203] |  |
| 13 | Spent LIB | shredding sieving alkali leaching roasting acid leaching filtration jarosite precipitation manganese dioxide precipitation copper hydroxide precipitation pH adjustment Li-Ni solvent extraction stripping of cobalt precipitation of cobalt oxalate | Cobalt oxalate |  | [26] |  |
| 7 | Spent LIBs | roasting mixing smelting reduction refining water atomizing leaching filtration | Co/Ni recovery |  | [42] |  |
| 4 | Spent LIBs | pilot scale crushing oxygen-free roasting water leaching filtration | Mn3O4 |  | [43] |  |
| 4 | Spent LIBs | pyro-metallurgy smelting leaching deep recycling techniques | Li, Co, Ni, Mn, Fe as oxides, salts or hydroxides |  | [44] |  |
| 3 | Spent LIBs | smelter granulation Co, Ni refining | Ni(OH)2, LiMeO2 |  | [28] |  |
| 6 | Spent LIBs | discharging dismantling discharging crushing screening incineration/pyrolysis | Cathode material, anode material, Cu, Al, Fe | Overview flowchart | [45] |  |
| 4 | Spent LIB | dismantling vacuum pyrolysis and condensation physical separation vacuum pyrolysis | Li meal and Co alloy | Overview flowchart | [270] |  |
| 4 | Spent LIB | smelter magnetic separation acid leaching solvent extraction precipitation | Co products and Ni products | Overview flowchart | [270] |  |
|  | Spent LIB | discharging battery liquid nitrogen freezing and crushing internal material of vehicle battery first stage pyrolysis pyrolysis residue crushing 2nd stage pyrolysis |  |  | [95] |  |
| 8 | Spent LIB | vacuum pyrolysis comminution size separation density separation magnetic separation agglomeration pyrometallurgy slag/dust leaching | Ni, Co ± Mn alloy Lithium Mn, Al | Accurec | [92] |  |
| 2 | Spent LIB | pyrometallurgy hydrometallurgy | Cu, Co, Fe, Ni | Umicore | [92] |  |
| 3 | Li-ion, NiMH, battery scrap, slag forming agent | smelter leaching refining | Co, Ni, Cu products for new batteries | Umicore | [38] |  |
| 8 | Spent batteries | cryogenic cooling shredder hammermill filter tank carbon filter press evaporator & storage tank array mixing tank filter press | Li2CO3 | Toxco | [38] |  |
| 4 | LIB | disassembling to cell auto-thermal pyrolysis multistep subsequent and linked mechanical treatment vacuum evaporation of Li/ entraining gas evaporation of Li | Lithium metal. Lithium oxide | EcoBatRec | [39,267] [39] [267] |  |
| 8 | Spent batteries | cryogenic cooling shredder hammermill filter tank carbon filter press evaporator & storage tank array mixing tank filter press | Li2CO3 | Toxco | [38] |  |
| Hydro-metallurgical Route |  |  |  |  |  |  |
| 4 | Spent LIB | broken in inert atmosphere magnetic separation leaching precipitation | Co products and Li products | Overview flowchart | [94] |  |
| 6 | Spent LIBs | battery deactivation battery component separation pre-treatment of active electrode material leaching process sepapration of metals from leaching solution further refining to battery grade | Li, Co, Ni, Mn, Fe |  | [261] |  |
| 7 | Scrap batteries | dismantling crushing leaching filtration solvent extraction scrubbing stripping | Co Sol |  | [46] |  |
| 7 | LIB electronic powder | leaching precipitation (pH 3.8) solvent extraction Ni recovery evaporation cooling Li recovery | Li2CO3 | Wastewater treatment | [47] |  |
| 6 | Spent LIBs | pre-treatment reductive leaching precipitating of Ni precipitating of Co extraction of Mn precipitating of Li | Li3PO4 |  | [48] |  |
| 5 | Leach liquor | purification DMG Co-loaded D2EHPA (NH4)2C2O4 carbonation | Recovery of Co & Li2CO3 |  | [48] |  |
| 13 | Spent LIB | dismantling crushing thermal treatment screening leaching with alkalis calcination dissolved with H2SO4 + H2O2 filtration precipitation filtration solvent extraction stripping of Co chemical deposition with oxalate | CoC2O4 |  | [49] |  |
| 7 | Spent LIB | discharging (NaCl) dismantling separation mechanical process/ NaOH dissolution/ solvent dissolution/ ultrasonic separation/ thermal treatment acid leaching filtration precipitation/ solvent extraction/ ion exchange resin/ electrochemical process/ regeneration | n.a. | Overview flowchart | [50] |  |
| 9 | Battery system | discharge disassembly crushing drying 1st air-classification 2nd crushing sieving leaching precipitation | LiOH, LiCO3 | LithoRec | [51] |  |
| 4 | Battery for recycle | shredding screening leaching solvent extractions | Separated salts | Overview flowchart | [15] |  |
| 5 | Spent LIBs | disassembly leaching pH adjustment precipitation precursor preparation | Li2CO3, Ni-Mn-Co precipitate |  | [53] |  |
| 5 | Spent LIBs | disassembly selective leaching sieving pH adjustment precipitation | Li2CO3, residual solution |  | [52] |  |
| 6 | Co, Li, Fe, Mn, Ni, Cu | leaching precipitation pH 5.5 solvent extraction stripping carbonatation Li crystallization | Co, Ni, Mn, Li |  | [54] |  |
| 6 | Co, Li, Fe, Mn, Ni, Cu | leaching precipitation pH 5.5 carbonatation Li crystallization | Co, Ni, Mn, Li |  | [54] |  |
| 7 | Batteries | discharge shredding magnetic separation dissolved aluminum in NaOH sieving density separation leaching | leachate |  | [55] |  |
| 4 | Batteries | gas blanket comminution size separation hydrolysis and filtration hydrometallurgical extractions | Recovered material | Overview flowchart | [17] |  |
| 6 | Spent LIBs | discharging dismantling ultrasonic cleaning leaching reactor filtration extraction of metals | n. a. |  | [56] |  |
| 7 | Cathode materials of spent LIBs | alkaline leaching reductive roasting carbonated water leaching acid leaching purification solvent extraction evaporation | NiSO4 · 6H2O, CoSO4 · 7H2O, MnSO4 · H2O |  | [57] |  |
|  | Hybrid cathode powder | leaching flotation 1st precipitation 2nd precipitation | MnO2, Mn2O3, Li3PO4 |  | [58] |  |
| 4 | Spent LIBs | dismantling peeling off cathode material from current collector leaching by inorganic acid, organic acid or microorganisms chemical precipitation/ electrochemical deposition/ solvent extraction | New materials, chemical products, metals | Overview flowchart | [18] |  |
| 4 | Spent LIBs | crushing screening leaching by inorganic acid, organic acid or microorganisms chemical precipitation/ electrochemical deposition/ solvent extraction | New materials, chemical products, metals | Overview flowchart | [18] |  |
| 5 | Spent LIBs | crushing ultrasonic washing screening leaching by inorganic acid, organic acid or microorganisms chemical precipitation/ electrochemical deposition/ solvent extraction | New materials, chemical products, metals | Overview flowchart | [18] |  |
| 3 | NCA particles | leaching oxidative precipitation neutralization | Ni(OH)2, Li-solution |  | [59] |  |
| 4 | LIB powder | leaching 1st precipitation 2nd precipitation calcination | Co3O4 |  | [60] |  |
| 7 | Spent LFP batteries | crushing in inert atmosphere physical separation fine screening leaching at 80 °C precipitation at 60 °C neutralization pH < 8.5 precipitation | Li3PO4 |  | [22] |  |
| 6 | Spent LFP | discharge separation alkaline leaching selective leaching 2 h at 60 °C 1st precipitation 2nd precipitation |  |  | [22] |  |
| 11 | Spent LIBs | discharge < 2 V shredding magnetic separation leaching 2 M NaOH drying screening leaching 2h at 65 – 70 °C precipitation co-precipitation NMC(OH)2 mixing and ball milling sintering 900 °C for 15 h in air | NMC |  | [22] |  |
| 7 | LFP/graphite or LFP/LTO spent batteries | binder dissolution carbon flotation leaching at 80 °C and pH 2 for 8 h oxidation precipitation resin precipitation | Li2CO3 |  | [22] |  |
| 9 | LCO spent batteries | discharging dismantling NMP ultrasonic heat treatment 2 h at 800 °C leaching 60 min at 80 °C pH adjustment LCO electro deposition washing drying | LiCoO2 | Collection of electrolyte | [22] |  |
| 7 | Spent LFP batteries | discharging dismantling sonication in water for 1 h ball milling for 2 h leaching 20 min precipitation pH 1.5 9 h at 90 °C precipitation pH 7 | Li3PO4 |  | [22] |  |
| 5 | Spent LFP batteries | discharge dismantling selective leaching 120 min at 25 °C precipitation re-synthesis | LFP-C | Precursor production | [22] |  |
| 6 | Spent LFP batteries | discharge dismantling selective leaching 30 min at 50 °C sieving carbothermal reduction scrubbing | LFP-C |  | [22] [61] |  |
| 7 | Spent LFP batteries | discharge dismantling PVDF dissolution and NMP filtration LFP drying 1 h at 100 °C grinding leaching 1 h at 80 °C and 60 g/L ionic sieve extraction | Li |  | [22] |  |
|  | Spent LIBs | discharge dismantling separation treated with NMP at 60 °C for 1 h calcine 700 °C for 5 h acid leaching reactor filtration reactor | Cobalt and lithium solution |  | [62] |  |
| 8 | Spent LIBs | dismantling discharging separation detachment thermal treatment reductive leaching adjustment of pH electrochemical deposition | LiCoO2 |  | [63] |  |
| 10 | Spent LIBs | discharging dismantling separation crushing NMP 100 °C for 1 h filtration calcine 700 °C for 5 h grinding for 2 h acid leaching filtration | Cobalt and lithium solution |  | [64] |  |
| 8 | Spent LFP batteries | discharging disassembling dilute alkali leaching acid leaching purifying concentration solution washing drying | Li3PO4 |  | [65] |  |
| 9 | Spent LIB | discharging physical separation crushing NMP 100 °C for 1h filtration calcination, 700 °C for 5 h grinding for 2h leaching reactor filtration | Cobalt & lithium solution |  | [66] |  |
| 7 | Spent LIB | discharging dismantling separating calcination 700 °C 5 h grinding 5 h metal leaching filtration | Pink filtrate and black residue |  | [67] |  |
| 7 | leachate | mixing hydrothermal reaction 200 °C for 8 h heating drying pre-heating calcination grinding | Powder sample |  | [68] |  |
| 4 | Spent LIB | manual dismantling physical separation 1st leaching Series of precipitation steps | CoC2O4 · 2H2O MnCO3, NiCO3, Li2CO3 |  | [69] |  |
| 10 | Spent LIB | discharging dismantling separating uncurling cutting ultrasonic washing with NPM filtration calcination, 700 °C 2h leaching with tartaric acid & ascorbic acid at 80 °C 5h filtration | Co | Wastewater treatment | [70] |  |
| 9 | Spent LIBs | discharging dismantling separating crushing ultrasonic washing with NPM filtration calcination, 700 °C, 2 h leaching with glycine & ascorbic acid 80 °C, 6h filtration | Cobalt-oxalate |  | [71] |  |
| 10 | n.a. | shredding electrolyte extraction magnetic separation zig-zag classifier thermal treatment air jet sieving leaching precipitation ratio adjustment sintering | Cathode material | LithoRec | [72,73] [72] [73] |  |
| 9 | LIB | dismantling separation of foils separation of Al foil and active material solution-based (NMP or NaOH dissolution) calcination leaching cathode resynthesizes from leachate remove impurities, adjust molar ratio of leachate for desire cathode sol-gel or coprecipitation synthesis | Cathode material | Overview flowchart | [74] |  |
| 9 | LIB | dismantling separation of foils separation of Al foil and active material solution-based (NMP or NaOH dissolution) calcination leaching purification selective precipitation/ solvent extraction recover metal as salts adjust molar ratio solid state synthesis | Cathode material |  | [74] |  |
| 4 | Spent LFP batteries | discharging dismantling oxidation leaching evaporation | Li2CO3 | In a further process chain the following substances are recovered: Anode plates Na2SO4 · H2O FePO4 Aluminum scrap | [75] |  |
| 5 | Spent LIB | sorting by type disassembling autothermal pyrolysis multi-step mechanical processes vacuum evaporation or selective entraining gas evaporation of Li | Li, metal oxide | electrolyte condensation | [33] |  |
| 9 | Spent batteries | cryogenic cooling shredding screening Li-leaching filtering Li salt precipitation filtering hybrid electric cell carbonation | Li2CO3 | Electrolyte recovery | [33] |  |
| 6 | Spent LIB | shredding neutralizing discharging from enclosed chamber pyrolyzing screening hydrometallurgical process | Metal fraction | Off gas cleaning | [33] |  |
| 8 | Spent batteries | rotary milling impact milling screening Li leaching in water filtering Acidic leaching Solution purification Co oxidation/ Co electrolysis | Co or Co2O3 | In a further process chain the following substances are recovered: Li2CO3 | [33] |  |
| 7 | Batteries | discharge shredding magnetic separation dissolving aluminum in NaOH sieve powders density separation leaching | Leachate |  | [76] |  |
| 6 | Spent LIBs | discharging dismantling separating vacuum pyrolysis acid leaching filtration | Cobalt oxalate and carbon; Lithium and aluminum solution |  | [77] |  |
| 6 | Spent LIBs | discharging dismantling separating vacuum pyrolysis acid leaching filtration | Cobalt and lithium solution, carbon |  | [77] |  |
| 7 | Spent LIB | rotary shear impact mill vibrating screen screen hydrolysis leaching electrolysis | Co, Li2CO3, Li3PO4 |  | [26] |  |
| 4 | Spent LIB | 1st cutting mill step 2nd cutting mill step magnetic separator leaching | Fe, Cu, Co |  | [26] |  |
| 14 | Spent LIB | discharging shredding magnetic separation dissolving sieving 1st leaching 1st precipitation 2nd leaching 2nd precipitation 3rd leaching 3rd precipitation 4th leaching 4th precipitation mixing and stirring with Li2CO3 | NMC | In a further process chain the following substances are recovered: LiFeO4 | [26] |  |
| 9 | Spent LIB | discharging manual disassembly 1st crushing drying air classification 2nd crushing sieving leaching precipitation calcination | Cathode material |  | [26] |  |
| 10 | Spent LIB | discharging disassembly case perforation shredding sieving/ magnetic separation dense media separation basic leaching purification Li adjustment dissolution filtration | Cathode material | Electrolyte recovery | [26] |  |
| 4 | Spent LIB | dismantling leaching liquid-liquid extraction recovery of valuable metals | Valuable metals |  | [78] |  |
| 8 | Spent batteries | shredding magnetic separation sieving water density separation secondary grinding leaching L/S separation solvent extraction | Mn-products Co-products Ni-product | Lithium precipitation Li2CO3 | [79] |  |
| 5 | Electrode powder | leaching Cu cementation Al, Fe precipitation Co, Ni, Mn precipitation Li2CO3 crystallization | Li2CO3 | Cathode metal salts, Al(OH)3, FeOOH (Goethite) | [80] |  |
| 10 | Leaching solution | adjust pH value filtration 1st adding extraction agent 1st separation 1st detection of pH 2nd adding extraction agent 2nd separation 2nd detection of pH chemical deposition precipitation | Cobalt oxalate |  | [91] |  |
| 10 | Spent LIB | pre-treatment alkali leaching reductive acid leaching removal of copper, deposition with Na2S removal of aluminum and iron neutralization precipitation 1st solvent extraction 2nd solvent extraction scrubbing stripping crystallization | CoSO4, NiSO4 | Controlled crystallization to NMC | [82] |  |
| 14 | Spent batteries | discharge disassembly shredding calcination physical separation leaching filtrating adjustment composition co-precipitation drying grinding calcining electrode materials mixing | Cathode material |  | [83] |  |
| 10 | Spent LIB | discharge dismantle vacuum pyrolysis peeled malic acid leaching filtration adjusting composition sol-gel formation dried calcined | Refreshed LNCM |  | [84] |  |
| 9 | Spent LIBs | discharging dismantling separating drying primary crushing secondary crushing sieving grain size separation ammoniacal leaching | Leachate |  | [84] |  |
| 8 | Spent LIBs | discharging manually disassemble crushing screening leaching filtration drying flotation | n.a. |  | [85] |  |
| 5 | Spent LIBs | dismantling separation alkaline leaching/ NMP ultrasonic treatment leaching solvent extraction/ precipitation/ electro-chemistry | Li, Co, Ni, Mn, Fe as oxides, salts or hydroxides | Overview flowchart | [44] |  |
| 7 | Spent LIBs | discharging dismantling separating mechanical/ physical method or thermal method thermal method/acid leaching/ ultrasonic renovation precipitation solvent extraction | Co and Li products | Comparing flow chart | [86] |  |
| 8 | Spent LIBs | cryogenic cooling shredder hammer mill filter tank carbon filter press evaporation & storage tank array mixing tank filter press | Li2CO3 |  | [28,87,88] |  |
| 5 | Spent LIBs | discharging dismantling separation the cathode materials citric acid leaching with H2O2 leaching solution | n.a. |  | [88] |  |
| 8 | Spent LIBs | discharging dismantling separation burning grinding formic acid leaching filtration dried | Filtrate |  | [87] |  |
| 10 | Spent LIBs | discharging dismantling alkali soluble filtering residue screening leaching FePO4 precipitation extractant removal co-precipitation | NiCoMn(OH)2 and Li2CO3 | Electrolyte recovery LIB manufacturing | [89] |  |
| 13 | Spent LIB | discharging dismantling crushing heat treatment removes the adhesive (600 °C for 1 h) vibration sieve 1st leaching 1st filtering 1st washing 1st drying 2nd leaching 2nd filtering 2nd washing 2nd drying | FePO4 and Li2CO3 |  | [90] |  |
| 6 | Spent LIB scrap | Acid leaching Removal of Fe, Al by D2EHPA Removal of cu by selective precipitation Extraction of Co by SX with Cyanex 272 Stripping Evaporization and crystallization | CoSO4 | Lithium recovery route Mass balance | [175] |  |
| 9 | Spent LIB | Discharging Dismantling Cathode and anode separation Milling Sieving Microwave reduction Water leaching CO2 purging | Li2CO3 |  | [261] |  |
| 9 | Spent LIB | discharging disassembly gas blanket comminution vacuum drying mixing density separation second comminution size separation hydrometallurgy | Cathode elements salts | Duesenfeld | [92] |  |
| 6 | Spent LIB | gas blanket comminution second comminution size separation hydrolysis filtration hydrometallurgy | Cathode elements salts | Recuply | [92] |  |

Table S.  7: Recycling efficiency and degree of purity of different LIB recycling routes.

| Input | Recovered material | Recycling efficiency [%] | Degree of purity [%] | Sources |
| --- | --- | --- | --- | --- |
| Direct physical |  |  |  |  |
| Electrode material | Cathode material | 96.88 | - | [32] |
| Battery electrodes | Cathode material | 99.5 % |  | [169] |
| Active material + carbon | Active materials | 99.3 |  | [93] |
| Active material | Active material | 97.1 | - | [166] |
| Battery systems |  | 75 | - | [21] [51] |
| New LIB | Cu | 73.6 | - | [185] |
| Spent LIB | Cu | 59.8 | - |  |
| Pyrolytic LFP material | LFP | 70.71 | 88.21 | [192] |
| Cathode material | Co & Li | 100 | - | [183] |
| Active material | Coating powder | 97.1 | 0.1 % Al impurity | [166] |
| Spent LIB | Cu | 95.9 | - | [193] |
| Spent LIB | Co Mn Cu Al | 97.66 96.66 90.14 86.29 | - | [182] |
| Spent LIB | Co Mn Cu Al | 98.99 89.45 94.95 87.83 | - | [167] |
| Active material | LiCoO2 | 89.83 | 91.75 | [170] |
| Active material | LiCoO2 | 96.88 | 93.89 | [27] |
| Spent LIB | Co Li Graphite | 95.72 98.93 91.05 | - | [37] |
| LFP batteries | LFP | 92.52 | - | [164] |
| Spent LIBs | Cu Co Al | 90.44 94.39 94.14 | - | [30] |
| Spent LIB | LiCoO2 | 86.97 | 98.00 | [31] |
| Spent LIB | LiCoO2 graphite | 49.32 73.56 | 97.19 82.57 | [187] |
| Spent LIB | Cathode material Anode material | 69.13 93.89 | At least 2.09 % impurities 93.89 | [32] |
| Spent LFP batteries | LFP | 49.67 | 88.67 % | [34] |
| Scrap material | Al foil | 88.6 | 74.8 | [180] |
| Pyro-metallurgical route |  |  |  |  |
| Input | Recovered material | Recycling efficiency [%] | Degree of purity [%] | Sources |
| Polymer LIB | Co Li | 99.84 | - | [42] |
| NMC batteries | Co Li | > 99 38.30 | - | [201] |
| Electrode material | Li as Li2CO3 Mn3O4 | 91.3 - | 99.7 95.11 | [43] |
| Active material | Li | 93.00 | “high grade material” | [41] |
| Electrode material | Li | 81.9 | - | [205] |
| Spent LCO cathode material | Li as Li3PO4 | 91.5 | - | [40] |
| Active material of spent LIB | Li and Co | Does not provide efficiency for the final step | - |  |
| Simulated slag | Li as LiCl | 97.45 | - | [196] |
| Spent LIB | Li as LiCO3 | 90 | 99.95 | [202] |
| Spent LIB | Co as CoCl2 Li as LiCl | 99.3 99.18 | - - | [197] |
| Simulated slag | Li as LiCl | 90.58 | - | [195] |
| Spent LCO batteries | Co Li | 95.72 98.93 | “high-purity product” | [37] |
| Portable LIB | Li as Li2CO3, Co alloy, Fe, Ni, Al, Cu, EMC, EC | 54,68 | - | [36] |
| Active material | Co Ni Mn Li | 98 99 99 73 | “batteriefähig” translates to battery grade | [271] |
| Simulated Slag | Li | 78.83 | - | [199] |
| Hydro-metallurgical route |  |  |  |  |
| Input | Recovered material | Recycling efficiency [%] | Degree of purity [%] | Sources |
| Spent LIBs | Li as Li2CO3 | 86 | 99.93 | [52] |
| Spent LIBs | Co as CoC2O4·2H2O Li as Li2CO3 | 91.2 62.13 | 0.32 % impurities 0.52 % impurities | [160] |
| Spent cathodic waste material | Mn as MnO2, Na0.55Mn2O4·1.5 H2O Co | 95 90 | - | [124] |
| Spent LIB | Li Ni Co | 91.77 89.64 88.14 | 99.3 98.9 99.5 | [126] |
| LCO | Li as Li3PO4 Co as CoC2O4 | 88 99 | 98.3 97.8 | [146] |
| Spent LIB | Li as Li2C2O4 Co as CoC2O4 | 98 97 | - | [157] |
| Spent cathode material | Li as LiF Co | 92.12 78.57 | 99.0 | [87] |
| Cathode scrap from LIB | Al as Al foil Li as Li2CO3 Ni Co Mn | 95.44 98.12 49.78 37.75 62.39 | 99.98 99.9 | [53] |
| Spent LCO LIB | Co | 84.55 | “contained unidentified impurities” | [150] |
| Spent LIBs | Co as CoC2O4·2H2O | 89.77 | 95.91 | [69] |
| Spent LIB | Ni as Ni-C4H8N2O2 Co as Co2C2O4·H2O Li as Li3PO4 | 92.15 92.15 88.11 | 98.46 96.47 99.07 | [48] |
| Spent NCA batteries | Co as Co2O3·3H2O Ni as Ni(OH)2 Li | 100 99.99 > 80 | 90.25 96.36 “good purity” | [48] |
| Electrode material of spent LIB | Co Cu Mn as MnO2 | 95.33 96.52 98.41 | 99.2 99.5 96 | [148] |
| Spent LIB | Li Co Mn Ni | 96.7 91.6 87.9 96.4 | - | [139] |
| Spent LIB | Co as Co3O4 CoC2O4 Ni as NiO Li as Li2CO3 | 78.4 83.3 88.2 71.28 | - 83 96 89 99.8 | [47] |
| Spent LIBs | Co Li | 94.8 98.5 | - | [137] |
| Spent LIBs | Co as Co3O4 Li as Li2CO3 | 98 99 | - | [81] |
| Spent LIB | Li as Li3PO4 Fe as FeCl3 Mn as MnO2/Mn2O3 | 80.93 85.4 81.02 | 99.32 97.91 98.73 | [58] |
| Spent LIB | Co as Co2C2O4·2H2O Li as Li3PO4 | 96.9 91.7 | 99.3 98.5 | [128] |
| Leach liquor | Co Mn Fe Cu Al | 81 92.5 94 99.2 95.6 | 99 99.7 | [142] |
| Spent LIB active material | Co | 95.59 | 99.5 | [125] |
| Spent LIB | Li | 80% | 98 | [54] |
| Spent LIB | Co as cobalt oxalate Li as lithium oxalate | 93.10 93.12 | 99 99 | [49] |
| Spent LIB | Li as Li2CO3 | 50 | 95 | [147] |
| Spent LIB | Co as Co3(PO4)2 only precipitation efficiency | 99 | 97.1 | [101] |

Table S.  8: Process energy of the different LIB recycling routes and single recycling steps.

| Direct physical |  |  |
| --- | --- | --- |
| Quote | Remarks on Process | Source |
| “[…] mechanical shredding and sizebased sorting, requires only a few pieces of equipment (i.e., shredder, vibration source, and sorting sieves) and low energy consumption […].” |  | [184] |
| “It [mechano-chemical process] can be performed at room temperature, which reduces energy consumption.” |  | [183] |
| “With every shredding batch an impulse frequency between 1 and 4 Hz can be set, which results in a relative energy consumption of 1.78 kWh/kg.” | Electro-hydraulic fragmentation | [168,173] |
| Calculated 13.6 kWh/battery or 6.92 kWh/kg | Discharge, disassembly, thermal heat, crushing, eddy current separation | [164] |
| “[…] the energy consumption per unit of mass of processed waste is about 0.033 kWh/kg.” | Pneumatic separation of anode and cathode material | [12] |
| “[…] the energy consumption per unit of mass of processed waste is about 6.924 kWh/kg.” | Discharge, disassembly, thermal heat, crushing, eddy current separation, Pneumatic separation | [13] |
| “A specific mechanical stress energy ws of 4.5 kWh/t was found to be sufficient to liberate housing, separator foil, anode foil, and cathode foil.” | Crushing | [186] |
| 0.3 kWh/kgmaterial | Akkuser Oy Process | [26] |
| “The cost of shredding process is electricity consumption and its cost is not high.” | Discharging, crushing, sieving | [31] |
| “The optimal milling time was determined to be 12 h based on energy consumption and conversion rates.” | Mechanochemical process | [183] |
| „It is worth noting that the high energy consumption of ball milling needs to be balanced with its productivity in the future development and application of this approach.” | Mechanochemical process | [28] |
| “The direct physical recycling process has the advantages of short recycling route, low energy consumption, environmental friendliness and high recovery rate.” | Review on direct physical, pyro- and hydrometallurgical processes | [18] |
| “Cryogenic treatment of LIBs and maintaining flow of inert gas (e.g., CO2, argon) might consume significant amount of electrical energy.“ | Review on commercial processes | [33] |
| “Mechanical treatment is characterized by its simplicity, efficiency, flexibility, and high throughput; however, it consumes considerable amount of energy (Huang et al.,2011 ).” | Adaption of minerals processes operation on battery recycling | [222,272] |
| “The use of vacuum chambers protects metals from the oxidation but requires a higher energy consumption, contrary to the enclosed vacuum environment, that starts the process at high vacuum degree avoiding continuous pressure monitoring (Xiao et al., 2017)” | Review on battery recycling | [43,260] |
| “Especially, using all recycled aluminum can reduce total energy consumption during electric vehicle production by 33%.[4c]” |  | [19,163] |
| Pyro-metallurgical |  |  |
| Quote | Remarks on Process | Source |
| “Traditional pyrometallurgical processes exhibit advantages of high efficiency and high productivity in the industry, but they involve high energy consumption, high cost, loss of materials, and emission of hazardous gases and dust” | -General information | [59,143,203] |
| “Furthermore, because inclosed vacuum environment had huge advantages over N2 pyrolysis and vacuum environments such as no lower energy consumption (no need to pump down continuously and no carrier gas), lower reaction pressure and no gas escape, there action environment was chosen as the inclosed vacuum conditions.” |  | [43] |
| “Therefore, considering the energy consumption and recovery efficiency, the optimal roasting temperature was selected to be 350 °C for the following study.” |  | [197] |
| “However, the aforementioned pyrometallurgical processes relied heavily on carbon-based reductants and operate at comparatively high temperatures resulting in significant CO2 evolution and intensive energy consumption during the recycling process.” | Thermokinetic analysis of pyro-metallurgical recycling | [198] |
| “Therefore, the high energy consumption resulted from the high temperature reduction and the low lithium concentration in water leaching solution seriously restrict the promotion and application of carbothermic reduction for industrial recycling of spent LIBs.” “The practice of lithium salt production indicates that the higher lithium concentration in the solution, the higher recovery efficiency and the lower energy consumption can be achieved.” | Carbothermic reduction and water leaching of lithium | [41] |
| “These results indicate that the spent cathode materials could be reduced efficiently by lignite in 0.5 h, which is beneficial to reduce energy consumption and promote production efficiency.” | Roasting and carbonated water leaching | [57] |
| “The plastics pyrolizing zone is operated at 700 °C, aiming to incinerate the plastic components of the spent LIBs to maintain the temperature and reduce the energy consumption of the smelting step.” “Pyrometallurgical process has some disadvantages such as materials loss, high energy consumption and hazardous gas (e.g dioxins, furans, etc.) release [31–33]. Therefore, alternative recycling processes with higher recovery rate, lower energy consumption and less environment hazards are needed to deal with a huge number of spent LIBs in the future.” | Review on direct physical, pyro- and hydrometallurgical processes | [18] |
| „Pyrometallurgical recycling can potentially result in a net increase in GHG emissions and energy consumption compared to raw material extraction, due to the incineration of nonvaluable battery components.37” | Review on recycling mixed cathode lithium ion batteries | [74] |
| „However, this technology has the main disadvantage of energy-consumption due to high temperature operation and associated to extra instruments for the control of toxic gases.“ | Commercial processes | [44] |
| “Other disadvantages of such technologies are low capacities, high energy consumption, as well as limited recycling efficiency [9,37,93].” | Review on recycling technologies | [17,53] |
| Hydro-metallurgical |  |  |
| Quote | Remarks on Process | Source |
| “hydrometallurgical processes are alternative solutions for the environmental problems and also consume less energy in comparison with pyrometallurgical processes.“ | Leaching organic acids | [130,137,143] |
| “Solvent extraction has some advantages such as low energy consumption, good separation effect and easy operational conditions.” “Chemical precipitation has the advantages of low cost and low energy consumption, but its applications may be discouraged by the difficulties in terms of the separation and recycling of metals from complicated solutions.” “When at a current density of 250 Am−2, 50 °C, pH value of 3–3.2, and with an electrolyte having about 50 g l-1 Ni and 20 g l-1 H3BO3 composition, nickel could be deposited with a current efficiency and a specific energy consumption of about 87 % and 2.96 kW h kg−1, respectively, leaving less than 100 ppm of nickel in the mother liquor.” “With the help of electrochemical deposition, high-purity metals and high recovery rate can be achieved; however, the energy consumption during this process is significant.” | Review on direct physical, pyro- and hydrometallurgical processes comparing solvent extraction, chemical precipitation and electrochemical deposition | [18,273] |
| „This method is of great interest for battery recycling research because it is known to be low cost, involves little energy consumption, and exhibits good environmental footprint [10].“ | Review on hydro-metallurgical and direct physical processes | [3,22] |
| “The energy consumption of leaching will be a function of the working temperature and time.” | Pretreatment, Ultrasonic washing, filtration, calcination, leaching, filtration, recovery of Co oxalate | [71] |
| “Electrochemical processes are attractive compared to conventional methods, since they are not energy intensive and the reaction occurs at a higher rate with minimum energy consumption.” | Electrochemical deposition | [78] |
| “This process has the advantages of easy operational conditions, low energy consumption and good separation effect.” | Solvent extraction | [274] |
| “Based on the above investigation and by considering the lower energy consumption, lower chemical consumption and relatively better leaching efficiency the best conditions for the leaching of cobalt and lithium from waste LiCoO2 were determined.” | Citric acid | [65] |
| “In particular yields of operation (leaching, purifications, product recovery), consumption of chemicals, energy requirements, and operation scheduling are estimated for each units according to experimental data reported: above.” | Simulation with and without solvent extraction | [54] |
| “A comparative analysis of inorganic and organic acids as well as bioleaching in terms of efficiency, environmental friendliness, cost, energy consumption, material consumption, and simple operation is also presented in Fig. 12f.” Fig. 12 f. shows that the energy consumption of bioleaching is lower compared to the leaching process using organic and inorganic acids. For organic and inorganic acid leaching the energy consumption is the same. “Electrodeposition has the advantage of achieving a high product purity because it does not introduce other impurities, but it has a high energy consumption because of the use of electricity.” | Comparing bioleaching and using organic or inorganic acids | [28] |
| „On the other hand, the solubility of Li2CO3 is inversely proportional to temperature. Therefore, the precipitation was usually carried out at a high temperature of more than 95 °C in order to precipitate Li2CO3 as much as possible. 58,59,115,124 Both of these two aspects lead to an increased energy consumption.“ | Review on hydro-metallurgical route | [234] |
| “The process has the advantages of low energy consumption and less recycling steps, and be feasible for recycling LIBs in large scale.” | Electrochemical deposition | [63] |
| “Considering the low energy consumption and relatively better reaction efficiencies, the suitable conditions were 80 °C and 120 min.“ | Organic oxalate as leachant and precipitant | [77] |
| “Obviously, the combined processes are of extreme prolixity and energy-consuming while cobalt is transferred from LiCoO2 to dissolving Co2+ in solution, and then precipitated Co2+.” | Organic oxalate leaching | [157] |
| „It can be also discovered from Table 2 that the leaching reaction can be finished in a short time of 20 min and only mild leaching conditions are required during leaching, which can greatly reduce the energy and chemical consumption.“ | Ascorbic acid leaching | [48] |
| “High recovery efficiencies of 99 % for both of cobalt and lithium were obtained with low energy and chemical consumption when the leaching process was carried out under the optimum conditions: 2M H2SO4, 5 vol.% H2O2, leaching time of 60min, leaching temperature of 80 °C and solid/liquid ratio of 50 g · L−1.” | Vacuum pyrolysis and hydrometallurgical recovery | [152] |
| „From the above-studied parameters and considering the lowest energy consumption, lowest chemical consumption and improved leaching efficiency, the best conditions for the leaching of cobalt and lithium from waste LiCoO2 was determined.“ | Leaching wuth DL-malic acid | [62] |
| The energy consumption for lithium recovery and organic removal was calculated based on the voltage of the cell during the first cycle (see the voltage profile in Fig. S2, ESI†). The energy efficiencies were 8.71 kWh/kgLi and 33.4 kWh/kgDOC for Li+ recovery and DOC removal, respectively. | Electrochemical wastewater treatment with lithium recovery after solvent extraction | [132] |
| „In the leaching process, the main consumption comes from the leaching agents and energy consumption. “ heating energy calculated to leach 1kg cathode material between 92.6 kWh (at H3PO4 0.7 M, 50 g/L 1,4% H2O2, 40 °C, 60 min, at Trifluoroacetic acid 15vol% acid, 12.5 g/L, 40 °C, 180 min) and 497 kWh (at H2SO4 1 M, 50 g/L, 95 °C, 240 min, at oxalic acid 1 M, 15 g/L, 95 °C, 150 min) | Economical comparison of different hydrometallurgical methods | [64,69,129,157,242] |
| „The whole recovery process is simpler and more environmentally friendly with low energy consumption compared with earlier methods.“ | Ascorbic acid leaching | [137] |
| “Therefore, the recovery rates of both Co and Li increased with the grinding degree of sample powders. Considering the energy consumption and recovery rates, it is recommended that 4 h is the optimum milling time.” | Milling, leaching and comparing different precipitants | [81] |
| “However, the marginal increase of leaching efficiency may be not deserved at the cost of a significant increase of energy consumption due to excessively high temperature.“ | Pretreatment, reductive leaching, metals recovery | [126] |
| “Energy consumption. The complete process to process the recycled Li-ion batteries is described in ESI.† [no further information] The energy required to recycle Li-ion batteries with the approach described is considerably less than the high temperature pyrometallurgical methods in use today. Energy is required to power the shredder, heat the batteries and acid to 70 °C for 1 hour during the leaching step, and heat the solution to 40 °C for 1 hour during the Li2CO3 precipitation step.” | Leaching, precipitation and active material mixing | [161] |
| “From the viewpoint of low energy consumption and high yield, we chose 60 °C as the optimum reaction temperature, with a duration of 40 min.” | Resynthesizing LNCM | [156] |
| “To achieve good crystalline materials of acceptable filterability, reaction is usually conducted at high temperature (80–90 °C) and requires long aging time. As a result, the NaF deposition method has disadvantages of consuming high reagents and energy, and is time consuming.” | Alkali leaching, reductive acid leaching, removal of copper, removal of Al and Fe, Solvent extraction | [82] |
| „These conditions result in low energy consumption, low chemical consumption, and better percentage leaching.“ | Succinic acid-based leaching | [67] |
| “here are lots of advantage by using hydrometallurgical treatments to extract valuable metals from solution as they are more flexible and reliable, eco- friendly, energy consumption is less, good rate of reaction, high purity and extract all the metals present in spent LIBs ” “As reported by Li et al., 2013, the energy consumption in producing citric acid is 35MJ/kg which is 1/10 of the energy required to produce same concentration of sulfuric acid or butane.” “The energy consumption of the process of recycling with organic acids (Fig.7) vis-à-vis inorganic acid (sulfuric) was calculated as 9.3 and 14 MJ/kg (Li et al., 2013).” | Review on hydro-metallurgical recycling | [139] |
| Fig. 14 | Organic acid leaching | [68] |

Table S.  9: Cumulative energy demand and global warming potential per functional unit of the different LIB recycling routes.

| Process | Impact Category | Result | Functional Unit | Reference |
| --- | --- | --- | --- | --- |
| Direct Physical Route |  |  |  |  |
| Direct | GWP (kg CO2 eq.) | 0.158 | 1 kg of battery | [243] |
|  | CED (MJ) | 3.3 |  |  |
| Direct | GWP (kg CO2 eq.) | 0.519 | 1 kg of spent battery | [244] |
|  | CED (MJ) | 3.9 |  |  |
| Direct | GWP (kg CO2 eq.) | 0.7 | 1 kg of recycled LFP batteries | [119] |
|  | CED (MJ) | 3.5 |  |  |
| Direct | CED (MJ) | 6 | 1 kg of LiCoO2 produced | [245] |
| Direct | CED (MJ) | 2468.83 | 1 tonne of LiMn2O4 | [275] |
| Intermediate Direct | CED (MJ) | 2848.65 | 1 tonne of Li2CO3 | [275] |
| Direct | CED (MJ) | 67.6 | 1 kg of battery | [19] |
| Intermediate Direct | CED (MJ) | 74.3 | 1 kg of battery | [19] |
| Process | Impact Category | Result | Functional Unit | Reference |
| Pyro-metallurgical Route |  |  |  |  |
| Pyrometallurgical | GWP (kg CO2 eq.) | 1.282 | 1 kg of battery | [243] |
|  | CED (MJ) | 14.5 |  |  |
| Pyrometallurgical | GHG (kg CO2 eq.) | 10.609 | 1 kg of cathode | [276] |
| Pyrometallurgical | GHG (kg CO2 eq.) | 1.41 | 1 kg of battery | [246] |
|  | CED (MJ) | 12.46 |  |  |
| Pyrometallurgical | GWP (kg CO2 eq.) | 185.61 | 1 LMO-NMC battery pack with nominal capacity of 11.4 kWh | [247] |
|  | CED (MJ) | 3151.5 |  |  |
| Pyrometallurgical | GWP 100 (kg CO2 eq.) | 680 | 1 tonne of battery | [251] |
| Pyrometallurgical | GWP (kg CO2 eq.) | 1167 | 1 tonne of battery | [120] |
|  | CED (MJ) | 14500 |  | EcoBatRec Process |
| Pyrometallurgical | GWP (kg CO2 eq.) | 1282 | 1 tonne of battery | [277] |
|  | CED (MJ) | 15313 |  | EcoBatRec Process |
| Pyrometallurgical | Embodied Energy (MJ) | 58.2 | 1 kg of NMC battery | [252] |
| Pyrometallurgical | GWP (kg CO2 eq.) | 0.0058 | 1 km | [253] |
|  | CED (MJ) | 0.0674 |  |  |
| Pyrometallurgical | CED (MJ) | 727.99 | 1 tonne of battery | [275] |
| Pyrometallurgical | GWP (kg CO2 eq.) | 4248 | 1 tonne of battery | [278] |
|  | CED (MJ) | 61277 |  | LiBRi process |
| Pyrometallurgical | CED (MJ) | 20.6 | 1 kg of battery | [254] |
| Process | Impact Category | Result | Functional Unit | Reference |
| Hydro-metallurgical Route |  |  |  |  |
| Hydrometallurgical | GWP (kg CO2 eq.) | 2.133 | 1 kg of battery | [243] |
|  | CED (MJ) | 35.5 |  |  |
| Hydrometallurgical | GWP (kg CO2 eq.) | 185.61 | 1 LMO-NMC battery pack with nominal capacity of 11.4 kWh | [247] |
|  | CED (MJ) | 3151.5 |  |  |
| Hydrometallurgical | GHG (kg CO2 eq.) | 4.21 | 1 kg of battery input | [248] |
|  | CED (MJ) | 15.2 |  |  |
| Hydrometallurgical | GHG (kg CO2 eq.) | 5.8 | 1 kWh of battery energy capacity | [249] |
|  | CED (MJ) | 148 |  |  |
| Hydrometallurgical | GHG (kg CO2 eq.) | 785.1 | 1 NMC battery pack | [250] |
|  | CED (MJ) | 2583.6 |  |  |
| Hydrometallurgical | GWP 100 (kg CO2 eq.) | 1320 | 1 tonne of battery | [251] |
| Hydrometallurgical | GWP (kg CO2 eq.) | 2133 | 1 tonne of battery | [121] |
|  | CED (MJ) | 35461 |  | LithoRec II process |
| Hydrometallurgical | GWP (kg CO2 eq.) | 2583 | 1 tonne of battery | [279] |
|  | CED (MJ) | 39078 |  | LithoRec II process |
| Hydrometallurgical | GWP (kg CO2 eq.) | 0.0058 | 1 km | [253] |
|  | CED (MJ) | 0.0674 |  |  |
| Hydrometallurgical | GWP (kg CO2 eq.) | 4.75 | 1 kg of recovered Co | [66] |
|  | CED (MJ) | 33 |  |  |
| Hydrometallurgical | CED (MJ) | 75 | 1 kg of battery | [19] |
| Hydrometallurgical | GWP (kg CO2 eq.) | 2494 | 1 tonne of battery | [280] |
|  | CED (MJ) | 37733 |  | LithoRec process |